Thermodynamic assessment of the Al–Mo–V ternary system
B. Hua,*, B. Yaoa, J. Wangb,*, J.-R. Zhaoc, F.-F. Mina, Y. Dub
a Anhui University of Science and Technology, School of Materials Science and Engineering, Huainan, China

b Central South University, State Key Laboratory of Powder Metallurgy, Changsha, China
c Shandong Academy of Sciences, Advanced Materials Institute, Shandong Key Laboratory for High Strength Lightweight Metallic Materials (HLM), Shandong Engineering Research Center for Lightweight Automobiles Magnesium Alloy, Jinan, China
* Corresponding author:

E-mail address: hubiao05047071@163.com (B. Hu); wangjionga@csu.edu.cn (J. Wang)
Abstract

Thermodynamic assessment of the Al–Mo–V ternary system was performed by means of the CALPHAD (CALculation of PHAse Diagram) approach based on the thermodynamic descriptions of three constitutive binary systems (Al–Mo, Al–V and Mo–V) as well as the experimental phase equilibria data available in the literature. The solution phases, i.e. liquid, bcc (Mo, V) and fcc (Al), were described using the substitutional solution models with the Redlich-Kister equation. The binary phases in the Al–Mo and Al–V systems with the solubilities of the third element were modeled using the sublattice models. An optimal set of thermodynamic parameters for the Al–Mo–V system was obtained. Six isothermal sections at 1200, 1000, 750, 715, 675 and 630 oC and liquidus projection with isotherm were calculated. The reaction scheme for the entire Al–Mo–V system was also constructed. Comparisons between the calculated and measured phase diagrams indicated that almost all the reliable experimental information was satisfactorily accounted for by the present modeling. 
Keywords: Al–Mo–V system; CALPHAD approach; Isothermal section; Liquidus projection
1. Introduction

Al–Mo–V ternary system is of great interest because it is an important sub-system in Al-based and Ti-based alloys. In Al-based alloys, Mo and V as two of the common additional elements improve the performance of the Al-based alloys 
 ADDIN EN.CITE 
[1-4]
. In Ti-based alloys, additions of transition metal elements such as Mo and V to titanium can stabilize the high temperature β phase to room temperature following rapid cooling. Mo and V are the most frequently used β isomorphous elements in Ti-based alloys [5]. In addition, Mo can improve the quenchability of the β phase in TiAl-based alloys 
 ADDIN EN.CITE 
[6,7]
 and V can improve the room-temperature ductility of TiAl and Ti3Al alloys [8]. The design of compositions of Al or Ti based novel alloys requires information about the phase equilibria of the Al–Mo–V ternary system. Therefore, a thorough thermodynamic assessment of the Al–Mo–V system is necessary for providing a set of reliable thermodynamic parameters for thermodynamic extrapolations to related higher order systems.
Thermodynamic description for the Al–Mo–V system is part of our efforts 
 ADDIN EN.CITE 
[9-17]
 to establish thermodynamic databases of multi-component Al and/or Ti based alloys. To the best of our knowledge, thermodynamic description for the Al–Mo–V system is not available in the literature nor in commercial database [18]. The purposes of the present work are to critically evaluate the measured phase diagram data available in the literature and to obtain a set of self-consistent thermodynamic parameters for the Al–Mo–V systems by means of the CALPHAD approach [19,20].
2. Evaluation of experimental data

To facilitate reading, the symbols used to denote the solid phases in the Al–Mo–V system are listed in Table 1. The Gibbs energy functions for the pure elements Al, Mo and V are taken from the SGTE (Scientific Group Thermodata Europe) database compiled by Dinsdale [21]. The thermodynamic parameters for Al–Mo, Al–V, and Mo–V systems are taken from Peng et al. [22], Gong et al. [23] and Zheng et al. [24], respectively. In particular, Peng et al. [22] refined the thermodynamic parameters of the Al–Mo system based on the work of Cupid et al.[7]. A set of thermodynamic parameters of the Mo–V binary system is taken from Zheng et al. [24] rather than the newer one from Bratberg and Frisk [25]. On the one hand, the thermodynamic parameters of the Mo–V system from Zheng et al. [24] are consistent with the multi-component alloys database developed by our research group [16]. On the other hand, the calculated results from Bratberg and Frisk show a miscibility gap in the bcc phase below 1160 K with no experimental evidence. For the Al–V system, the thermodynamic parameters are adopted from our own group [23] rather than Lindahl et al.[26] also in order to be consistent with the database of our group. The calculated three constitutive binary systems are presented in Fig. 1 (a) to (c).
Table 1 Summary of crystal structures of solid phases in the Al–Mo–V system.

	Phase/Temperature range (oC)
	Prototype
	Pearson

symbol
	Space

group
	Phase description

	(Al), < 660
	Cu
	cF4
	
[image: image1.wmf]3

Fmm


	Solid solution based on fcc_A1 Al

	(Mo), < 2623
	W
	cI2
	
[image: image2.wmf]3

Imm


	Solid solution based on bcc_A2 Mo

	(V), < 1910
	W
	cI2
	
[image: image3.wmf]3

Imm


	Solid solution based on bcc_A2 V

	Al12Mo, < 712
	Al12W
	cI26
	
[image: image4.wmf]3

Im


	Solid solution based on Al12Mo

	Al5Mo, < 845
	Al5W
	hP12
	P63
	Solid solution based on Al5Mo

	Al22Mo5, < 940
	Al22Mo5
	oF216
	Fdd2
	Solid solution based on Al22Mo5

	Al17Mo4, < 997
	Al17Mo4
	mC84
	C2
	Solid solution based on Al17Mo4

	Al4Mo, 941~1152
	Al4W
	mC30
	Cm
	Solid solution based on Al4Mo

	Al3Mo, 791~1222
	Al3Mo
	mC32
	C2/m
	Solid solution based on Al3Mo

	Al8Mo3, < 1528
	Al8Mo3
	mC22
	C2/m
	Solid solution based on Al8Mo3

	Al63Mo37, 1489~1569
	‒
	‒
	‒
	Binary phase Al63Mo37

	AlMo, 1470~1721
	W
	cI2
	
[image: image5.wmf]3

Imm


	Solid solution based on bcc_A2

	AlMo3, < 2148
	Cr3Si
	cP8
	
[image: image6.wmf]3

Pmn


	Solid solution based on AlMo3

	Al21V2, < 688
	Al21V2
	cF176
	
[image: image7.wmf]3

Fdm


	Solid solution based on Al21V2

	Al45V7, < 719
	Al45V7
	mC104
	C2/m
	Solid solution based on Al45V7

	Al23V4, < 734
	Al23V4
	hP54
	P63/mmc
	Solid solution based on Al23V4

	Al3V, < 1222
	Al3Ti
	tI8
	I4/mmm
	Solid solution based on Al3V

	Al8V5, < 1413
	Cu5Zn8
	cI52
	
[image: image8.wmf]43

Im


	Solid solution based on Al8V5


[image: image9.jpg]°C

o

Temperature

2800

2400+

20004

1600

—_—

N

o

o
I

Liquid

997

/ \
AlesMo37 AlMo
1222

AlsMo~ LA I3Mo

941

845

800

712

~

91 -

660

400-

AD

661

Al17Mo4

| AlsMo Al22Mos
AlsMos3

Al

i\)_Alleo

I
0.4 0.6 0.8 1.0
Wegiht fraction Mo Mo



 [image: image10.jpg]®) 5000

1600 Liquid B
| 1413 (V) B
@)
o 1222
8'\ 1200_ —
=
= B o
3
= 809 i
= 660664 | % -+ AlsVs B
= H g =
S I i
0 | | | |
0 0.2 0.4 0.6 0.8 1.0
Al Weight fraction V V

1910




[image: image11.jpg]Temperature

(Mo,V)

Liquid

1910

0.2

Weight fraction V

|
0.4

|
0.6

0.8

1.0




Fig. 1 Calculated binary phase diagrams: (a) Al–Mo system [22], (b) Al–V system [23], and (c) Mo–V system [24].
The phase equilibria data of the Al–Mo–V system were mainly experimentally determined by Sperner [27] and Raman [28]. In 1959, six isothermal sections at 1200, 1000, 750, 715, 675 and 630 oC were investigated by Sperner [27]. According to these isothermal sections, no ternary compound was found in the Al–Mo–V system. The binary phases AlMo3, Al8Mo3, Al3Mo, Al5Mo and Al12Mo in Al–Mo binary side and Al8V5, Al3V, Al6V (or Al23V4, Al45V7) and Al21V2 in Al–V binary side were detected in the work of Sperner [27]. The solubilities of Mo in Al8V5 and Al3V and V in AlMo3 and Al8Mo3 slightly decrease with temperature ranges from 1200 to 630 oC. The solubilities of Mo in Al6V, Al21V2, Al3Mo, Al5Mo and Al12Mo are nearly constant in temperature ranges. The average solubilities of Mo in Al8V5, Al3V, Al6V and Al21V2 are about 30, 25, 10 and 6.5 wt.%, respectively, and the ones of V in AlMo3, Al8Mo3, Al3Mo, Al5Mo and Al12Mo are about 20, 11, 6, 3 and 1.5 wt.%, respectively, in temperature ranges from 1200 to 630 oC. The solubilities of Mo in Al–V binary phases and V in Al–Mo binary phases decrease with the decreasing of temperature. Nine invariant reactions, i.e. L + (Mo, V) ↔ Al8V5 + AlMo3 at about 1600 oC, L + AlMo3 ↔ Al8V5 + Al8Mo3 at 1450 oC, L + Al8V5 ↔ Al3V + Al8Mo3 at 1300 oC, L + Al8Mo3 ↔ Al3V + Al3Mo at 1100 oC, L + Al3Mo ↔ Al3V + Al5Mo at 720 oC, L + Al3V ↔ Al6V + Al5Mo at 700 oC, L + Al5Mo ↔ Al6V + Al12Mo at 690 oC, L + Al6V ↔ Al21V2 + Al12Mo at 680 oC, and L ↔ Al12Mo + Al21V2 + (Al) at 656 oC, were reported and a tentative reaction scheme for the Al–Mo–V system was also constructed by Sperner [27] on the basis of the isothermal sections. The experimental data measured by Sperner [27] are included in the present optimization due to the consistency of these isothermal sections.
Twenty ternary alloys were prepared and the isothermal section at 1000 oC was detemined by Raman [28]. According to the experimental results [28], the binary phases AlMo3, Al8Mo3, Al4Mo and Al5Mo in Al–Mo binary side and Al8V5 and Al3V in Al–V binary side were detected. A ternary compound Al14Mo5V closing to the binary compound Al8Mo3 was reported by Raman [28]. Later, Virkar and Raman [29] carried out the crystallographic investigations showing that the Al14Mo5V phase has a similer structure with the Al8Mo3 phase and believed that the so-called ternary phase Al14Mo5V is the solid solution of the alloying element V in Al8Mo3. Hence, the Al14Mo5V phase is not included in the present optimization. In addition, the phase relations of the isothermal section at 1000 oC reported by Raman [28] are inconsistent with the ones from Sperner [27]. Hence, the experimental phase diagram data reported by Raman [28] is not used in the thermodynamic optimization but only used for comparison.
3. Thermodynamic model
The phases in the Al–Mo–V system to be optimized in this work are as follows: solution phases, liquid, bcc (Mo, V) and fcc (Al); binary phases extending into the ternary system, Al12Mo, Al5Mo, Al22Mo5, Al17Mo4, Al4Mo, Al3Mo, Al8Mo3, AlMo3, Al21V2, Al45V7, Al23V4, Al3V and Al8V5. Different models were employed to describe the above mentioned phases.
3.1 Solution phases

The solution phases, i.e. liquid, bcc (Mo, V) and fcc (Al) are described by the substitutional solution model. The molar Gibbs energy of solution phase 
[image: image12.wmf]f

(
[image: image13.wmf]f

= liquid, bcc or fcc) is expressed by the Redlich-Kister-Muggianu polynomial [30]: 


[image: image14.wmf]oooo

AlAlMoMoVV

AlAlMoMoVV

AlMoAl,MoAlVAl,VMoVMo,V

012

AlMoVAlAl,Mo,VMoAl,Mo,VVAl,Mo,V

(lnlnln)

()

m

GxGxGxG

RTxxxxxx

xxLxxLxxL

xxxxLxLxL

ffff

fff

fff

=×+×+×

+×××+×+×

+××+××+××

+××××+×+×

              (1)

where R is the gas constant, 
[image: image15.wmf]Al

x

, 
[image: image16.wmf]Mo

x

 and 
[image: image17.wmf]V

x

 are the molar fractions of the elements Al, Mo and V, respectively. The standard element reference (SER) state [21], i.e. the stable structure of the element at 25 (C and 1 bar, is used as the reference state of Gibbs energy. The parameters 
[image: image18.wmf],

(,Al,Mo,V)

ij

ij

L

f

=

 are the interaction parameters from binary systems. The ternary interaction parameters 
[image: image19.wmf]0

Al,Mo,V

L

f

, 
[image: image20.wmf]1

Al,Mo,V

L

f

and 
[image: image21.wmf]2

Al,Mo,V

L

f

are linearly temperature-dependent, which can be expressed as
[image: image22.wmf]Al,Mo,V

L=A+BT

f

×

. The coefficients A and B will be optimized from experimental data in the present work. 
3.2 Binary phases

According to the experimental data from Sperner [27] and Raman [28], the binary phases Al12Mo, Al5Mo, Al3Mo, Al8Mo3 and AlMo3 in the Al–Mo system and Al21V2, Al6V (or Al23V4, Al45V7), Al3V and Al8V5 in the Al–V system exhibit some solubilities for V and Mo, respectively. Sublattice models [31,32] are used to describe these binary phases and listed in Table 2. In view of the experimental results [27,28], it is assumed that Mo and V substitute each other in the sublattice models. In accordance with the formula for sublattice model, the Gibbs energy of Al12Mo, modeled as Al12(Mo, V)1, taking as an example can be expressed as:


[image: image23.wmf](

)

121212

1212

AlMoAlMoAlMo

ooo

MoAl:MoVAl:V

MoMoVV

AlMoAlMo

01

MoVAl:Mo,VAl:M

1

M

V

oV

o,

(lnln)

...

GyGyG

RTyyyy

y

y

yL

y

L

¢¢¢¢

=×+×

¢¢¢¢¢¢¢¢

+×××+×

éù

¢¢¢¢

+××

¢¢¢¢

-

++

ëû

                     (2)

where 
[image: image24.wmf]Mo

y

¢¢

 and 
[image: image25.wmf]V

y

¢¢

 are the site fractions of Mo and V in the second sublattice. The parameters 
[image: image26.wmf]12

AlMo

o

Al:Mo

G

 and 
[image: image27.wmf]12

AlMo

o

Al:V

G

 correspond to the Gibbs energies of the end-members Al12Mo and Al12V, respectively. The interaction parameters 
[image: image28.wmf]12

AlMo

0

Al:Mo,V

L

 and 
[image: image29.wmf]12

AlMo

1

Al:Mo,V

L

 are also linearly temperature-dependent, which can be expressed as
[image: image30.wmf]12

AlMo

Al:Mo,V

L=a+bT

×

, and the coefficients a and b will be optimized in the present work. 

It is noted that the AlMo3 and Al8V5 phase are modeled as (Al, Mo, V)0.75(Al, Mo, V)0.25 and (Al, V)2(Al, Mo, V)3(Mo, V)2(Al)6, respectively. The boldfaces mean the normal atoms (i.e. major species) in the sublattices. The Al22Mo5, Al17Mo4 and Al4Mo phases were not determined by Sperner [27]. In view of the solubilities of V in other bianry phases in the Al–Mo system, these phases were described as (Al)22(Mo, V) 5, (Al)17(Mo, V) 4, and (Al)4(Mo, V) 1, respectively, in the present work. Analogous expressions like Eq. (2) are applied to describe the Gibbs energies of the AlMo3, Al8V5, Al22Mo5, Al17Mo4, and Al4Mo phases.
4. Results and discussions
The thermodynamic parameters are evaluated by the optimization module PARROT [33] in the program Thermo-Calc software, which works by minimizing the square sum of the differences between the measured and calculated values. The step-by-step optimization procedure described by Du et al. [34] is utilized in the present assessment.

The optimization begins with the isothermal section at 1200 oC. According to the solubilities of V in the Al8Mo3 and AlMo3 phases and Mo in the Al3V and Al8V5 phases and the phase relations at 1200 oC determined by Sperner [27], the interaction parameters a for the Al8Mo3, AlMo3, Al3V and Al8V5 phases in Eq.(2) are optimized. Then, the isothermal sections at 1000, 750, 715, 675 and 630 oC are considered one by one in the optimization. Next, the temperatures of invariant reactions reported by Sperner [27] are evaluated. The ternary interaction parameters A for the liquid and bcc_A2 phases in Eq.(1) are obtained by fitting the experimental data of invariant reactions. Finally, all the parameters are optimized simultaneously. The thermodynamic parameters obtained in the present work are listed in Table 2.
Table 2 Summary of the thermodynamic parameters for the Al–Mo–V systema
	Phase/Model
	Thermodynamic parameters
	Reference

	Liquid: 
Model (Al, Mo, V)1
	
[image: image31.wmf]0Liquid

Al,Mo

102047.637.780

LT

=-+×



[image: image32.wmf]1Liquid

Al,Mo

13754.51.889

LT

=-×



[image: image33.wmf]2Liquid

Al,Mo

37326.310.402

LT

=-+×



[image: image34.wmf]0Liquid

Al,V

122625.817.400

LT

=-+×



[image: image35.wmf]1Liquid

Al,V

51463.00.850

LT

=-×



[image: image36.wmf]0Liquid

Mo,V

1613.00.187

LT

=--×



[image: image37.wmf]0Liquid

Mo,V

158.00.104

LT

=--×



[image: image38.wmf]0Liquid

Al,Mo,V

112576.6

L

=-


	[22]
[22]
[22]
[23]
[23]
[24]
[24]
This work

	fcc_A1:
Model (Al, Mo, V)1Va1
	
[image: image39.wmf]0fcc_A1

Al,Mo:Va

146174.575.699

LT

=-+×



[image: image40.wmf]0fcc_A1

Al,V:Va

95812.028.3

LT

=-+×


	[7]
[23]

	bcc_A2: 
Model (Al, Mo, V)1Va3
	
[image: image41.wmf]0bcc_A2

Al,Mo:Va

73113.322.770

LT

=-+×



[image: image42.wmf]1bcc_A2

Al,Mo:Va

16584.5

L

=-



[image: image43.wmf]2bcc_A2

Al,Mo:Va

18877.2

L

=-



[image: image44.wmf]0bcc_A2

Al,V:Va

136730.014.400

LT

=-+×



[image: image45.wmf]1bcc_A2

Al,V:Va

131633.043.000

LT

=-×



[image: image46.wmf]0bcc_A2

Mo,V:Va

4011.71.455

LT

=-+×



[image: image47.wmf]1bcc_A2

Mo,V:Va

187.10.208

LT

=+×



[image: image48.wmf]0bcc_A2

Al,Mo,V:Va

6573.8

L

=+


	[7]
[7] 
[7]
[23]
[23]
[24]
[24]
This work

	Al12Mo: 
Model (Al)12(Mo, V) 1
	
[image: image49.wmf]12

AlMo

oofccobcc

Al:MoAlMo

147884.533.00012

GTGG

=-+×+×+



[image: image50.wmf]12

AlMo

oofccobcc

Al:VAlV

81391.512

GGG

=-+×+


	[22]
This work

	Al5Mo:
Model (Al)5(Mo, V) 1
	
[image: image51.wmf]5

AlMo

oofccobcc

Al:MoAlMo

148908.138.35

GTGG

=-+×+×+



[image: image52.wmf]5

AlMo

oofccobcc

Al:VAlV

83221.85

GGG

=-+×+


	[22]
This work

	Al22Mo5: 
Model (Al)22(Mo, V) 5
	
[image: image53.wmf]225

AlMo

oofccobcc

Al:MoAlMo

745899.1198.5225

GTGG

=-+×+×+×



[image: image54.wmf]225

AlMo

oofccobcc

Al:VAlV

380000225

GGG

=-+×+×


	[22]
This work

	Al17Mo4: 
Model (Al)17(Mo, V) 4
	
[image: image55.wmf]174

AlMo

oofccobcc

Al:MoAlMo

596728.1160.4174

GTGG

=-+×+×+×



[image: image56.wmf]174

AlMo

oofccobcc

Al:VAlV

305000174

GGG

=-+×+×


	[22]
This work

	Al4Mo: 
Model (Al)4(Mo, V) 1
	
[image: image57.wmf]4

AlMo

oofccobcc

Al:MoAlMo

145502.135.4154

GTGG

=-+×+×+



[image: image58.wmf]4

AlMo

oofccobcc

Al:VAlV

750004

GGG

=-+×+


	[22]
This work

	Al3Mo: 
Model (Al)3(Mo, V) 1
	
[image: image59.wmf]3

AlMo

oofccobcc

Al:MoAlMo

143801.440.9333

GTGG

=-+×+×+



[image: image60.wmf]3

AlMo

oofccobcc

Al:VAlV

79031.63

GGG

=-+×+


	[22]
This work

	Al8Mo3: 
Model (Al)8(Mo, V)3
	
[image: image61.wmf]83

AlMo

oofccobcc

Al:MoAlMo

432300128.34183

GTGG

=-+×+×+×



[image: image62.wmf]83

AlMo

oofccobcc

Al:VAlV

240072.083

GGG

=-+×+×


	[22]
This work

	Al63Mo37: 
Model (Al)63(Mo)37
	
[image: image63.wmf]6337

AlMo

oofccobcc

Al:MoAlMo

1515523.6176.0586337

GTGG

=--×+×+×


	[22]

	AlMo3: 
Model (Al, Mo, V)0.75(Al, Mo, V)0.25
	
[image: image64.wmf]3

AlMo

oofcc

Al:AlAl

10000

GG

=+



[image: image65.wmf]3

AlMo

oofccobcc

Al:MoAlMo

100000.750.25

GGG

=+×+×



[image: image66.wmf]3

AlMo

oofccobcc

Mo:AlAlMo

21181.03.3390.250.75

GTGG

=-+×+×+×



[image: image67.wmf]3

AlMo

oobcc

Mo:AlMo

10000

GG

=+



[image: image68.wmf]3

AlMo

o

Al,Mo:Al

0.456

GT

=×



[image: image69.wmf]3

AlMo

o

Mo:Al,Mo

2.633

GT

=-×



[image: image70.wmf]3

AlMo

oobcc

V:VV

10000

GG

=++



[image: image71.wmf]3

AlMo

oofccobcc

Al:VAlV

0.750.25

GGG

=+×+×



[image: image72.wmf]3

AlMo

oofccobcc

V:AlAlV

32696.40.250.75

GGG

=-+×+×



[image: image73.wmf]3

AlMo

oobccobcc

Mo:VMoV

0.750.25

GGG

=+×+×



[image: image74.wmf]3

AlMo

oobccobcc

V:MoMoV

0.250.75

GGG

=+×+×



[image: image75.wmf]3

AlMo

o

Mo,V:Al

11863.4

G

=+


	[7] 
[7]
[7]
[7]
[7]
[7]
This work
This work

This work

This work

This work

This work

	Al21V2: 
Model (Al)21(Mo, V)2
	
[image: image76.wmf]212

AlV

oofccobcc

Al:VAlV

191571.68.28212

GTGG

=--×+×+×



[image: image77.wmf]212

AlV

oofccobcc

Al:MoAlMo

199397.7212

GGG

=-+×+×


	[23]
This work

	Al45V7: 
Model (Al)45(Mo, V)7
	
[image: image78.wmf]457

AlV

oofccobcc

Al:VAlV

670493.219.240457

GTGG

=--×+×+×



[image: image79.wmf]457

AlV

oofccobcc

Al:MoAlMo

701507.1457

GGG

=-+×+×


	[23]
This work

	Al23V4: 
Model (Al)23(Mo, V)4
	
[image: image80.wmf]234

AlV

oofccobcc

Al:VAlV

383139.09.100234

GTGG

=--×+×+×



[image: image81.wmf]234

AlV

oofccobcc

Al:MoAlMo

435847.736.765234

GTGG

=-+×+×+×


	[23]
This work

	Al3V: 
Model (Al)3(Mo, V)1
	
[image: image82.wmf]3

AlV

oofccobcc

Al:VAlV

95784.20.5203

GTGG

=-+×+×+



[image: image83.wmf]3

AlV

oofccobcc

Al:MoAlMo

129979.436.9443

GTGG

=-+×+×+



[image: image84.wmf]3

AlV

o

Al:Mo,V

8089.97

G

=-


	[23]
This work
This work

	Al8V5: 
Model (Al, V)2(Al, Mo, V)3(Mo, V)2(Al)6
	
[image: image85.wmf]85

AlV

oofccobcc

Al:Al:V:AlAlV

100000112

GGG

=+×+×



[image: image86.wmf]85

AlV

oofccobcc

V:Al:V:AlAlV

528219.926.00094

GTGG

=-×+×+×



[image: image87.wmf]85

AlV

oofccobcc

Al:V:V:AlAlV

454220.026.00085

GTGG

=-+×+×+×



[image: image88.wmf]85

AlV

oofccobcc

V:V:V:AlAlV

26000.067

GGG

=-+×+×



[image: image89.wmf]85

AlV

o

Al,V:Al:V:Al

465244.0

G

=-



[image: image90.wmf]85

AlV

o

Al,V:V:V:Al

465244.0

G

=-



[image: image91.wmf]85

AlV

o

Al:Al,V:V:Al

299767.0

G

=-



[image: image92.wmf]85

AlV

o

V:Al,V:V:Al

299767.0

G

=-



[image: image93.wmf]85

AlV

oofccobcc

Al:Mo:Mo:AlAlMo

85

GGG

=+×+×



[image: image94.wmf]85

AlV

oofccobcc

Al:Al:Mo:AlAlMo

112

GGG

=+×+×



[image: image95.wmf]85

AlV

oofccobccobcc

Al:V:Mo:AlAlMoV

823

GGGG

=+×+×+×



[image: image96.wmf]85

AlV

oofccobccobcc

V:Mo:Mo:AlAlMoV

652

GGGG

=+×+×+×



[image: image97.wmf]85

AlV

oofccobccobcc

V:Mo:V:AlAlMoV

634

GGGG

=+×+×+×



[image: image98.wmf]85

AlV

oofccobccobcc

V:Al:Mo:AlAlMoV

922

GGGG

=+×+×+×



[image: image99.wmf]85

AlV

oofccobccobcc

V:V:Mo:AlAlMoV

625

GGGG

=+×+×+×



[image: image100.wmf]85

AlV

oofccobccobcc

Al:Mo:V:AlAlMoV

420988.667.328832

GTGGG

=-+×+×+×+×



[image: image101.wmf]85

AlV

o

Al:Mo,V:V:Al

147052.5

G

=-


	[23]
[23]
[23]
[23]
[23]
[23]
[23]
[23]
This work

This work

This work

This work

This work

This work

This work

This work

This work


a All parameters are given in J/(mole-atoms); Temperature (T) in K. The Gibbs energies for the pure elements Al, Mo and V are taken from the SGTE database compiled by Dinsdale [21]. 
In figure 2, the calculated isothermal section at 1200 oC of the Al–Mo–V system is compared with the observed one by Sperner [27]. As can be seen from these figures, the calculated results can account for most of the experimental data [27] in view of experimental errors. It is noteworthy that there is a sharp edge on the AlMo3 phase in the two-phase region AlMo3 + bcc (Mo, V) at 1200 oC in Fig. 2(b). It can be interpreted by the following two reasons. On the one hand, the shape of AlMo3 is determined by the thermodynamic parameters of both the AlMo3 phase and other phases around AlMo3, which are globally optimized based on the phase equilibria data. On the other hand, a sharp edge on the AlMo3 phase in the two-phase region AlMo3 + bcc (Mo, V) is expected to exist at a temperature above 1000oC. This can be deduced from the difference between the phase relations of the isothermal sections at 1200 and 1000 oC. A miscibility gap of bcc (Mo) + bcc (V) appears at 1000 oC in Fig. 3. Thus, there exists the three-phase region of AlMo3 + bcc (Mo) + bcc (V). The compositions of AlMo3 for the two three-phase regions AlMo3 + bcc (Mo) + bcc (V) and AlMo3 + Al8V5 + bcc (V) at 1000 oC are not identical and the miscibility gap of bcc (Mo) + bcc (V) disappears above 1000 oC. In other words, the three-phase region of AlMo3 + bcc (Mo) + bcc (V) does not exist above 1000 oC. Hence, based on the phase rule, there should be a sharp edge on the AlMo3 in the two-phase region AlMo3 + bcc (Mo, V) at the temperatures above 1000 oC, which will disappear at higher temperatures. The exact temperature should be measured in the future experiments, which is not the purpose of the present work.
[image: image102.jpg](a) \Y4
T=1200°C 4 g

N AlsMo3 N AlMos 7Y

/\
9 0.2 0.4 0.6 0.8 1.0
Al Weight fraction Mo Mo



[image: image103.jpg](b) \%
T=1200°C 1

F. Sperner (1959):
O One-phase region
D Two-phase region

A Three-phase region





Fig. 2 Observed and calculated isothermal section at 1200 oC of the Al–Mo–V system: (a) observed section by Sperner [27] and (b) calculated section according to the present work along with the experimental data from Sperner [27].
[image: image104.jpg]T=1000°C \%
1.0

O @ A F.Sperner (1959):
OO A A.Raman (1966):
O ®  One-phase region
@ © Two-phase region

A A  Three-phase region





Fig. 3 Calculated isothermal section at 1000 oC of the Al–Mo–V system, compared with the experimental data from Sperner [27] and Raman [28].
Figure 3 shows the calculated isothermal section at 1000 oC in comparison with the experimental data reported by Sperner [27] and Raman [28]. The calculations can reproduce most of the experimental data from Sperner [27]. The Al4Mo phase was not found at 1000 oC in the work of Sperner [27], which is inconsistent with the accepted Al–Mo phase diagram [22], as shown in Fig.1 (a). The calculated three-phase regions liquid + Al4Mo + Al3V and Al4Mo + Al3V + Al3Mo need further experimental verifications. As mentioned above, the experimental data from Raman [28] are not used in the present optimization but only used for comparison due to the contradictions of the experimental results between Sperner [27] and Raman [28]. In addition, the present calculations show that there exists a miscibility gap of bcc (Mo) + bcc (V) closing to the Mo–V binary side below 1000 oC. The existence of the miscibility gap also needs to be confirmed by further experiments.
In figure 4, the calculated isothermal section at 750 oC is compared with the experimental data from Sperner [27]. In comparison with the experimental data, some discrepancies exist in Al–Mo binary side. According to the experimental data from Sperner [27], the binary phase Al3Mo was determined but the Al5Mo, Al22Mo5 and Al17Mo4 phases not at 750 oC. The experimental results are inconsistent with the accepted Al–Mo binary phase diagram in Fig.1 (a). The Al5Mo, Al22Mo5 and Al17Mo4 phases are stable at 750 oC but Al3Mo not. Thus, the phase relations liquid + Al3Mo + Al3V and Al3Mo + Al8Mo3 + Al3V reported by Sperner [27] are modified to be liquid + Al5Mo + Al3V, Al5Mo + Al22Mo5 + Al3V, Al22Mo5 + Al17Mo4 + Al3V, and Al17Mo4 + Al8Mo3 + Al3V in the present work. In addition, due to the existence of the miscibility gap of bcc (Mo) + bcc (V), the calculated composition (i.e. 10 wt.% Mo and 70 wt.% V) of the bcc (V) phase for the three-phase region AlMo3 + Al8V5 + bcc (V) deviates from the experimental one of 44.7 wt.% Mo and 47.6 wt.% V by Sperner [27]. It leads to three data points of half-black circle in V-rich corner in two-phase region of Al8V5 + bcc (V) measured by Sperner [27] to be in three-phase region of Al8V5 + bcc (V) + AlMo3 in the present work.
[image: image105.jpg]T=750°C v

F. Sperner (1959):
O One-phase region
D Two-phase region

A Three-phase region





Fig. 4 Calculated isothermal section at 750 oC of the Al–Mo–V system, compared with the experimental data from Sperner [27].
[image: image106.jpg]T=715°C v

F. Sperner (1959):
O One-phase region
D Two-phase region

A Three-phase region





Fig. 5 Calculated isothermal section at 715 oC of the Al–Mo–V system, compared with the experimental data from Sperner [27].
Figure 5 presents the calculated isothermal section at 715 oC along with the experimental data from Sperner [27]. Just as the isothermal section at 750 oC, there are some discrepancies between the calculated and experimental isothermal section at 715 oC. Besides the issues of the Al22Mo5 and Al17Mo4 phases and the miscibility gap of bcc (Mo) + bcc (V) mentioned above, the calculated phase relations in Al-rich corner along the Al–V binary side are inconsistent with the experimental data reported by Sperner [27]. The Al6V binary phase was determined in the isothermal section at 715 oC by Sperner [27]. Actually, the Al6V phase is replaced by the Al23V4 and Al45V7 phases in the accepted Al–V phase diagram [23] in Fig.1 (b). Hence, the phase relations liquid + Al6V + Al3V and liquid + Al5Mo + Al3V reported by Sperner [27] are modified to be liquid + Al5Mo + Al45V7, Al5Mo + Al45V7 + Al23V4, and Al5Mo + Al23V4 + Al3V in the present work.
[image: image107.jpg]F. Sperner (1959):
O One-phase region
P Two-phase region

A Three-phase region




  [image: image108.jpg](b) \%
T=630°C 1.

F. Sperner (1959):
O One-phase region
D Two-phase region

A Three-phase region





Fig. 6 Calculated isothermal sections of the Al–Mo–V system along with the experimental data from Sperner [27]: (a) 675 °C and (b) 630 °C.

The calculated isothermal sections at 675 and 630 oC of the Al–Mo–V system in comparison with the experimental data from Sperner [27] are shown in Fig. 6 (a) and (b), respectively. As can be seen from this figure, most of the reliable experimental data reported by Sperner [27] can be reproduced well by the present modeling except for the phase relations of the Al22Mo5, Al17Mo4, Al23V4 and Al45V7 phases and the miscibility gap of bcc (Mo) + bcc (V) mentioned above. The calculated phase relations at 675 oC are the same with the ones at 630 oC except for the liquid (Al) at 675 oC and fcc (Al) at 630 oC. 
Based on the above discussion, almost all the reliable experimental phase diagram data are satisfactorily accounted for by the present modeling except for the phase relations of the Al4Mo, Al22Mo5, Al17Mo4, Al23V4 and Al45V7 phases and the miscibility gap of bcc (Mo) + bcc (V). According to the experimental data from Sperner [27], the Al4Mo, Al22Mo5 and Al17Mo4 phases were not determined and the Al23V4 and Al45V7 phases were replaced by the Al6V phase. The results of Sperner [27] do not agree with the accepted Al–Mo and Al–V binary phase diagrams, as shown in Fig.1 (a) and (b), respectively. Thus, the calculated and experimental isothermal sections show some differences. Further experiments are needed to confirm the accuracy of the calculated phase relations related to these binary phases Al4Mo, Al22Mo5, Al17Mo4, Al23V4 and Al45V7. Furthermore, the calculated isothermal sections show there is a miscibility gap of bcc (Mo) + bcc (V) closing to the Mo–V binary side below 1000 oC. Further experiments are also necessary to verify the existence of the miscibility gap.
Table 3 Calculated temperatures for the invariant reactions on the liquidus surface in the Al–Mo–V system compared with the experimental values. 
	Type
	Invariant Reaction
	Temperature/ºC
	Source

	U1
	L + Al63Mo37 ↔ Al8Mo3 + AlMo
	1502
	Calculated (This work)

	U2
	L + AlMo ↔ Al8Mo3 + AlMo3
	1409
	Calculated (This work)

	U3
	L + Al8Mo3 ↔ Al8V5 + AlMo3
	1334
	Calculated (This work)

	E1
	L + (Mo, V) ↔ Al8V5 + AlMo3
L ↔ Al8V5 + AlMo3 + (Mo, V)
	~ 1600

1329
	Measured [27]
Calculated (This work)

	P1
	L + Al8V5 ↔ Al3V + Al8Mo3
L + Al8V5 + Al8Mo3 ↔ Al3V
	~ 1300

1292
	Measured [27]
Calculated (This work)

	U4
	L + Al8Mo3 ↔ Al3V + Al3Mo
	~ 1100

1102
	Measured [27]
Calculated (This work)

	U5
	L + Al3Mo ↔ Al3V + Al4Mo
	1069
	Calculated (This work)

	U6
	L + Al4Mo ↔ Al3V + Al17Mo4
	995
	Calculated (This work)

	U7
	L + Al17Mo4 ↔ Al3V + Al22Mo5
	910
	Calculated (This work)

	P2
	L + Al3V + Al22Mo5 ↔ Al5Mo
	904
	Calculated (This work)

	U8
	L + Al3V ↔ Al6V + Al5Mo

L + Al3V ↔ Al23V4 + Al5Mo
	700

717
	Measured [27]
Calculated (This work)

	U9
	L + Al23V4 ↔ Al45V7 + Al5Mo
	715
	Calculated (This work)

	U10
	L + Al5Mo ↔ Al6V + Al12Mo

L + Al5Mo ↔ Al45V7 + Al12Mo
	690

703
	Measured [27]
Calculated (This work)

	U11
	L + Al6V ↔ Al21V2 + Al12Mo

L + Al45V7 ↔ Al21V2 + Al12Mo
	680

683
	Measured [27]
Calculated (This work)

	U12
	L ↔ Al12Mo + Al21V2 + (Al)

L + Al21V2 ↔ Al12Mo + (Al)
	656

664
	Measured [27]
Calculated (This work)


On the basis of the optimization of the experimental data reported by Sperner [27], the liquidus projection with isotherm of the Al–Mo–V system is also calculated in the present work, as shown in Fig. 7 (a). Fig.7 (b) is the enlargement of the triangle in Fig. 7 (a) and Fig.7 (c) is the enlargement of the circle in Fig. 7 (b). A comparison between the calculated and literature reported invariant reactions is listed in Table 3. Figure 8 presents the partial reaction scheme for the Al–Mo–V system. A general agreement is obtained between the calculations and the experiments [27]. For the type of the invariant reactions, the calculated invariant reactions are L ↔ Al8V5 + AlMo3 + (Mo, V), L + Al8V5 + Al8Mo3 ↔ Al3V, and L + Al21V2 ↔ Al12Mo + (Al), whereas the reported ones [27] are L + (Mo, V) ↔ Al8V5 + AlMo3, L + Al8V5 ↔ Al3V + Al8Mo3, and L ↔ Al12Mo + Al21V2 + (Al), respectively. For the temperatures of the invariant reactions, the calculated results are in good agreement with the reported ones within the estimated experimental errors except for the invariant reaction L ↔ Al8V5 + AlMo3 + (Mo, V). The difference between the calculated and the reported temperature of the invariant reaction L ↔ Al8V5 + AlMo3 + (Mo, V) is about 271 oC. Further experiments are needed to verify the type and temperature of the invariant reactions because these invariant reactions reported by Sperner [27] are tentative and obtained by considering the determined isothermal sections. In addition, Sperner [27] also reported two ternary invariant reactions L + AlMo3 ↔ Al8V5 + Al8Mo3 and L + Al3Mo ↔ Al3V + Al5Mo derived from binary invariant reactions L ↔ AlMo3+ Al8Mo3 at 1760 oC and L + Al3Mo ↔ Al5Mo at 735 oC in the Al–Mo system. According to the accepted Al–Mo phase diagram in Fig.1 (a), these binary invariant reactions do not exist. Thus, the ternary invariant reactions L + AlMo3 ↔ Al8V5 + Al8Mo3 and L + Al3Mo ↔ Al3V + Al5Mo reported by Sperner [27] are obviously wrong.
[image: image109.jpg](a) M

00

2300

N

pS
1200 2400
0 max 1
' T\| AlMos
Pi Al U 500
1100 sMos3
100 A,
0 Y= - el/\4p3\1 e N
0 0.2 0.4 AlaMasMo (g 8 1.0

Al Weight fraction Mo Mo




[image: image110.jpg](b)

/\p9

0.04

/\ps /N N pr/N

N\
0.08 0.12
Weight fraction Mo




 [image: image111.jpg]AV

6 /\
0.002

/N prI/\ N\ N\ N\

0.004 0.006
Weight fraction Mo

A
0.008




Fig. 7 Calculated liquidus surface projection in the Al–Mo–V system: (a) the whole composition, (b) enlarged triangle in (a), and (c) enlarged circle in (b).

The present work demonstrates that the CALPHAD approach is a powerful tool to evaluate a ternary system with limited experimental data. It is possible to describe the complicated phase equiliria of a system over the entire composition in a wide temperature range based on limited reliable experimental information. The CALPHAD approach is highly recommended in the present work. It is expected that this approach can be applied to other systems in order to develop reliable thermodynamic descriptions of multi-component alloys. 
[image: image112.jpg]Al-Mo Al-Mo-V Al-V
2148°C | p1
L+(Mo)=AlMo3
1721°Cc [ p2
L+AlMo3=AlMo
1569°C | p3
L+AlMo=Al63Mo037
1528°C | el
L=Al63Mo37+AlsMo3 A
[1502°c] L+alssMos=AlsMos+AIMo [ UI |
|
L+AlsMo3+AlMo AlesMo37+AlsMo3+AlMo
1413°C | P4

[1409°C] L+AIMo=AlsMos+AIMos | U2 ]

L+(V)=AlgVs

|
AlMo+AlsMo3+AIMo3 [ +AlsMo3+AlMo3

1391°C | €maxi

L=AlsMo3+Al8Vs

\ 4
[1334°c] L+AlsMos=Alsvs+AIMos [ Us |

|
L+AlsVs+AlMo3 AlsMo3+AlIsVs+AIMo3

1222°C [ Ps

K I

[1320°c] L=Alsvs+AIMos+(Mo,v) [E1 ]
T

AlgVs+AIMo3+(Mo, V)

[1202°C]  L+AlsMos+Alsvs=ALV [ P1 ]

I I
AlsMo3+AI8V5+AI3V L+Al8Vs+AIZV

L+AlsMo3=Al3Mo

1152°C | p7

1222°Cc | Ps

L+AlsMo3+AlV |

[1102°c [ L+AlsMos=ALV+ALMo | Us |
|

L+AlzMo=Al4Mo

997°Cc | ps

| AlsMo3+Al3V+AIZMo [+Al3V+AlI3Mo

[1069°C] L+ALMo=AlV+ALMo [ uUs |

AlZMo+AI3V+Al4Mo L+Al3V+Al4Mo

L+Al4aMo=Al17Mo4

940°C | po

v
[ 99s°c | L+AlsMo=ALV+AlITMos | Us |

AlaMo+AIZV+ALI7TMo4 [ +Al13V+AL17Mo4

L+Al17Mo4=Al22Mos

g45°C [ pio

| 910°C | L+Ali7Mo4=Al3V+Al22Mos |U7|
|
Al17Mo4+Al3V+Al22Mos L+ Al3V+Al22Mos

[ 904°c | L+aBv+AlMos=AIsMo [ P2 |

I I
L+Al22Mos+AlsMo Al3V+Al22Mos+AlsMo

L+AI8V5=Al3V

L+Al22Mos=AlsMo

712°C | pis

734°Cc | pn

| L+AlsMo+AlI3V

[717°C | L+AlV=AlsVa+AlsMo | Us]

L+Al23V4+AlsMo Al3V+AI23Va+AlsMo

L+A13V=Al23V4

719°Cc | pr2

v
[ 715°C [ L+Alsva=Alsvr+alsMo | us |

Al23Va+AlasVi+AlsMo  L+AlasV7+AlsMo

L+AlsMo=Al12Mo

661°C | pio

[ 703°c | L+alsMo=ALsv7+AlI2Mo [Uo]
|

I
L+Al4sV7+Ali2Mo AlsMo+Al4sV7+Ali2Mo

L+Al23V4=Al45V7

688°C_ | D14

I 683°C | L+Al4sV7=Al21V2+Al12Mo |U11|
|

|
L+Al21V2+Ali2Mo Al4sV7+Al21Va2+Ali2Mo

L+Al45V7=Al121V2

664°C | P13

v
[ 664°c | LrALiva=AlaMo+(AD  Jun]
I

T
L+A1121\|’10+(A1) Al21V2+Ali2Mo+(Al)

L+Ali2Mo=(Al)

L+Al21Va=(Al)





Fig. 8 Partial reaction scheme of the Al–Mo–V system according to the present work.
5. Conclusions
The experimental phase equilibria data for the Al–Mo–V system available in the literature are critically evaluated. Based on these experimental data, the Al–Mo–V system is evaluated by means of the CALPHAD approach. A set of self-consistent thermodynamic parameters of the Al–Mo–V system is obtained. Some representative isothermal sections and liquidus surface projection are calculated. The calculated results are in good agreement with the most of the experimental data. In spite of the fact that the CALPHAD method is a powerful tool to optimize a system based on the limited experimental data, no updated descriptions of the binary phases in the Al-Mo and Al-V systems in the work of Sperner [27] and the absence of the thermodynamic experimental data (such as mixing enthalpy, activity, etc.) in the Al–Mo–V system may lead to the obtained thermodynamic parameters in the present work failing to account for some new phase equilibria data and thermodynamic data. Therefore, further experiments are necessary to verify the phase relations related to the binary phases Al4Mo, Al22Mo5, Al17Mo4, Al23V4 and Al45V7 and the existence of the miscibility gap of bcc (Mo) + bcc (V). 
Acknowledgments

The financial support from the National Natural Science Foundation of China (Nos. 51501002 and 51601228), the China Postdoctoral Science Foundation (No. 2015M581972), and the Hunan Provincial Natural Science Foundation for Youth of China (No. 2016JJ3152) are greatly acknowledged.
Reference
[1] M. Eumann, M. Palm, G. Sauthoff, Intermetallics, 12 (2004) 625-633.

[2] H. Bei, E.P. George, Acta Mater., 53 (2005) 69-77.

[3] M. Dudová, K. Kuchařová, T. Barták, H. Bei, E.P. George, C. Somsen, A. Dlouhý, Scr. Mater., 65 (2011) 699-702.

[4] S. Milenkovic, A.A. Coelho, R. Caram, J. Cryst. Growth, 211 (2000) 485-490.

[5] G. Lutjering, J.C. Williams, Titanium, Springer, New York, 2007.

[6] I.S. Jung, H.S. Jang, M.H. Oh, J.H. Lee, D.M. Wee, Mater. Sci. Eng. A, 329-331 (2002) 13-18.

[7] D.M. Cupid, O. Fabrichnaya, F. Ebrahimi, H.J. Seifert, Intermetallics, 18 (2010) 1185-1196.

[8] X.G. Lu, N. Gui, A.T. Qiu, G.X. Wu, C.H. Li, Metall. Mater. Trans. A, 45A (2014) 4155-4164.

[9] J. Wang, H.H. Xu, S.L. Shang, L.J. Zhang, Y. Du, W.Q. Zhang, S.H. Liu, P.S. Wang, Z.-K. Liu, Calphad, 35 (2011) 191-203.
[10] B. Hu, W.-W. Zhang, Y.B. Peng, Y. Du, S.H. Liu, Y.L. Zhang, Thermochim. Acta, 561 (2013) 77-90.

[11] D. Hao, B. Hu, K. Zhang, L.J. Zhang, Y. Du, J. Mater. Sci., 49 (2014) 1157-1169.

[12] B. Hu, Y. Du, J.C. Schuster, W.H. Sun, S.H. Liu, C.Y. Tang, Thermochim. Acta, 578 (2014) 35-42.

[13] B. Hu, S. Qin, Y. Du, Z.Y. Li, Q.P. Wang, J. Phase Equilib. Diff., 36 (2015) 333-349.

[14] B. Hu, Y. Du, J.-J. Yuan, Z.-F. Liu, Q.-P. Wang, J. Min. Metall. Sect. B-Metall., 51(2) B (2015) 125–132.

[15] J. Zhao, J. Zhou, S. Liu, Y. Du, S. Tang, Y. Yang, J. Min. Metall. Sect. B-Metall., 52(1) B (2016) 99-112.

[16] B. Hu, J. Wang, C. Wang, Y. Du, J.B. Zhu, Calphad, 55 (2016) 103-112.
[17] B. Hu, X.M. Yuan, Y. Du, J. Wang, Z.-K. Liu, J. Alloys Compd., 693 (2017) 344-356.

[18] http://www.thermocalc.com.
[19] Z.-K. Liu, Y. Wang, Computational thermodynamics of materials, Cambridge University Press, Cambridge, 2016.

[20] H. Lukas, S.G. Fries, B. Sundman, Computational thermodynamics: the CALPHAD method, Cambridge University Press, Cambridge, 2007.

[21] A.T. Dinsdale, Calphad, 15 (1991) 317-425.

[22] J. Peng, P. Franke, D. Manara, T. Watkins, R.J.M. Konings, H.J. Seifert, J. Alloys Compd., 674 (2016) 305-314.

[23] W.P. Gong, Y. Du, B.Y. Huang, R. Schmid-Fetzer, C.F. Zhang, H.H. Xu, Z. Metallkd., 95 (2004) 978-986.

[24] F. Zheng, B.B. Argent, J.F. Smith, J. Phase Equilib., 20 (1999) 370-372.

[25] J. Bratberg, K. Frisk, Calphad, 26 (2002) 459-476.

[26] B. Lindahl, X.L. Liu, Z.-K. Liu, M. Selleby, Calphad, 51 (2015) 75-88.

[27] F. Sperner, Z. Metallkd., 50 (1959) 592-596 (in German).
[28] A. Raman, Z. Metallkd., 57 (1966) 535-540 (in German).
[29] A.V. Virkar, A. Raman, Z. Metallkd., 60 (1959) 594-600.

[30] O. Redlich, A.T. Kister, Ind. Eng. Chem., 40 (1948) 345-348.

[31] M. Hillert, L.I. Staffansson, Acta Chem. Scand., 24 (1970) 3618-3626.

[32] B. Sundman, J. Ågren, J. Phys. Chem. Solids, 42 (1981) 297-301.

[33] B. Sundman, B. Jansson, J.-O. Andersson, CALPHAD, 9 (1985) 153-190.

[34] Y. Du, R. Schmid-Fetzer, H. Ohtani, Z. Metallkd., 88 (1997) 545-556.



Table 1 Summary of crystal structures of solid phases in the Al–Mo–V system.

	Phase/Temperature range (oC)
	Prototype
	Pearson

symbol
	Space

group
	Phase description

	(Al), < 660
	Cu
	cF4
	
[image: image113.wmf]3

Fmm


	Solid solution based on fcc_A1 Al

	(Mo), < 2623
	W
	cI2
	
[image: image114.wmf]3

Imm


	Solid solution based on bcc_A2 Mo

	(V), < 1910
	W
	cI2
	
[image: image115.wmf]3

Imm


	Solid solution based on bcc_A2 V

	Al12Mo, < 712
	Al12W
	cI26
	
[image: image116.wmf]3

Im


	Solid solution based on Al12Mo

	Al5Mo, < 845
	Al5W
	hP12
	P63
	Solid solution based on Al5Mo

	Al22Mo5, < 940
	Al22Mo5
	oF216
	Fdd2
	Solid solution based on Al22Mo5

	Al17Mo4, < 997
	Al17Mo4
	mC84
	C2
	Solid solution based on Al17Mo4

	Al4Mo, 941~1152
	Al4W
	mC30
	Cm
	Solid solution based on Al4Mo

	Al3Mo, 791~1222
	Al3Mo
	mC32
	C2/m
	Solid solution based on Al3Mo

	Al8Mo3, < 1528
	Al8Mo3
	mC22
	C2/m
	Solid solution based on Al8Mo3

	Al63Mo37, 1489~1569
	‒
	‒
	‒
	Binary phase Al63Mo37

	AlMo, 1470~1721
	W
	cI2
	
[image: image117.wmf]3

Imm


	Solid solution based on bcc_A2

	AlMo3, < 2148
	Cr3Si
	cP8
	
[image: image118.wmf]3

Pmn


	Solid solution based on AlMo3

	Al21V2, < 688
	Al21V2
	cF176
	
[image: image119.wmf]3

Fdm


	Solid solution based on Al21V2

	Al45V7, < 719
	Al45V7
	mC104
	C2/m
	Solid solution based on Al45V7

	Al23V4, < 734
	Al23V4
	hP54
	P63/mmc
	Solid solution based on Al23V4

	Al3V, < 1222
	Al3Ti
	tI8
	I4/mmm
	Solid solution based on Al3V

	Al8V5, < 1413
	Cu5Zn8
	cI52
	
[image: image120.wmf]43

Im


	Solid solution based on Al8V5


Table 2 Summary of the thermodynamic parameters for the Al–Mo–V systema
	Phase/Model
	Thermodynamic parameters
	Reference

	Liquid: 
Model (Al, Mo, V)1
	
[image: image121.wmf]0Liquid

Al,Mo

102047.637.780

LT

=-+×



[image: image122.wmf]1Liquid

Al,Mo

13754.51.889

LT

=-×



[image: image123.wmf]2Liquid

Al,Mo

37326.310.402

LT

=-+×



[image: image124.wmf]0Liquid

Al,V

122625.817.400

LT

=-+×



[image: image125.wmf]1Liquid

Al,V

51463.00.850

LT

=-×



[image: image126.wmf]0Liquid

Mo,V

1613.00.187

LT

=--×



[image: image127.wmf]0Liquid

Mo,V

158.00.104

LT

=--×



[image: image128.wmf]0Liquid

Al,Mo,V

112576.6

L

=-


	[22]
[22]
[22]
[23]
[23]
[24]
[24]
This work

	fcc_A1:
Model (Al, Mo, V)1Va1
	
[image: image129.wmf]0fcc_A1

Al,Mo:Va

146174.575.699

LT

=-+×



[image: image130.wmf]0fcc_A1

Al,V:Va

95812.028.3

LT

=-+×


	[7]
[23]

	bcc_A2: 
Model (Al, Mo, V)1Va3
	
[image: image131.wmf]0bcc_A2

Al,Mo:Va

73113.322.770

LT

=-+×



[image: image132.wmf]1bcc_A2

Al,Mo:Va

16584.5

L

=-



[image: image133.wmf]2bcc_A2

Al,Mo:Va

18877.2

L

=-



[image: image134.wmf]0bcc_A2

Al,V:Va

136730.014.400

LT

=-+×



[image: image135.wmf]1bcc_A2

Al,V:Va

131633.043.000

LT

=-×



[image: image136.wmf]0bcc_A2

Mo,V:Va

4011.71.455

LT

=-+×



[image: image137.wmf]1bcc_A2

Mo,V:Va

187.10.208

LT

=+×



[image: image138.wmf]0bcc_A2

Al,Mo,V:Va

6573.8

L

=+


	[7]
[7] 
[7]
[23]
[23]
[24]
[24]
This work

	Al12Mo: 
Model (Al)12(Mo, V) 1
	
[image: image139.wmf]12

AlMo

oofccobcc

Al:MoAlMo

147884.533.00012

GTGG

=-+×+×+



[image: image140.wmf]12

AlMo

oofccobcc

Al:VAlV

81391.512

GGG

=-+×+


	[22]
This work

	Al5Mo:
Model (Al)5(Mo, V) 1
	
[image: image141.wmf]5

AlMo

oofccobcc

Al:MoAlMo

148908.138.35

GTGG

=-+×+×+



[image: image142.wmf]5

AlMo

oofccobcc

Al:VAlV

83221.85

GGG

=-+×+


	[22]
This work

	Al22Mo5: 
Model (Al)22(Mo, V) 5
	
[image: image143.wmf]225

AlMo

oofccobcc

Al:MoAlMo

745899.1198.5225

GTGG

=-+×+×+×



[image: image144.wmf]225

AlMo

oofccobcc

Al:VAlV

380000225

GGG

=-+×+×


	[22]
This work

	Al17Mo4: 
Model (Al)17(Mo, V) 4
	
[image: image145.wmf]174

AlMo

oofccobcc

Al:MoAlMo

596728.1160.4174

GTGG

=-+×+×+×



[image: image146.wmf]174

AlMo

oofccobcc

Al:VAlV

305000174

GGG

=-+×+×


	[22]
This work

	Al4Mo: 
Model (Al)4(Mo, V) 1
	
[image: image147.wmf]4

AlMo

oofccobcc

Al:MoAlMo

145502.135.4154

GTGG

=-+×+×+



[image: image148.wmf]4

AlMo

oofccobcc

Al:VAlV

750004

GGG

=-+×+


	[22]
This work

	Al3Mo: 
Model (Al)3(Mo, V) 1
	
[image: image149.wmf]3

AlMo

oofccobcc

Al:MoAlMo

143801.440.9333

GTGG

=-+×+×+



[image: image150.wmf]3

AlMo

oofccobcc

Al:VAlV

79031.63

GGG

=-+×+


	[22]
This work

	Al8Mo3: 
Model (Al)8(Mo, V)3
	
[image: image151.wmf]83

AlMo

oofccobcc

Al:MoAlMo

432300128.34183

GTGG

=-+×+×+×



[image: image152.wmf]83

AlMo

oofccobcc

Al:VAlV

240072.083

GGG

=-+×+×


	[22]
This work

	Al63Mo37: 
Model (Al)63(Mo)37
	
[image: image153.wmf]6337

AlMo

oofccobcc

Al:MoAlMo

1515523.6176.0586337

GTGG

=--×+×+×


	[22]

	AlMo3: 
Model (Al, Mo, V)0.75(Al, Mo, V)0.25
	
[image: image154.wmf]3

AlMo

oofcc

Al:AlAl

10000

GG

=+



[image: image155.wmf]3

AlMo

oofccobcc

Al:MoAlMo

100000.750.25

GGG

=+×+×



[image: image156.wmf]3

AlMo

oofccobcc

Mo:AlAlMo

21181.03.3390.250.75

GTGG

=-+×+×+×



[image: image157.wmf]3

AlMo

oobcc

Mo:AlMo

10000

GG

=+



[image: image158.wmf]3

AlMo

o

Al,Mo:Al

0.456

GT

=×



[image: image159.wmf]3

AlMo

o

Mo:Al,Mo

2.633

GT

=-×



[image: image160.wmf]3

AlMo

oobcc

V:VV

10000

GG

=++



[image: image161.wmf]3

AlMo

oofccobcc

Al:VAlV

0.750.25

GGG

=+×+×



[image: image162.wmf]3

AlMo

oofccobcc

V:AlAlV

32696.40.250.75

GGG

=-+×+×



[image: image163.wmf]3

AlMo

oobccobcc

Mo:VMoV

0.750.25

GGG

=+×+×



[image: image164.wmf]3

AlMo

oobccobcc

V:MoMoV

0.250.75

GGG

=+×+×



[image: image165.wmf]3

AlMo

o

Mo,V:Al

11863.4

G

=+


	[7] 
[7]
[7]
[7]
[7]
[7]
This work

This work

This work

This work

This work

This work

	Al21V2: 
Model (Al)21(Mo, V)2
	
[image: image166.wmf]212

AlV

oofccobcc

Al:VAlV

191571.68.28212

GTGG

=--×+×+×



[image: image167.wmf]212

AlV

oofccobcc

Al:MoAlMo

199397.7212

GGG

=-+×+×


	[23]
This work

	Al45V7: 
Model (Al)45(Mo, V)7
	
[image: image168.wmf]457

AlV

oofccobcc

Al:VAlV

670493.219.240457

GTGG

=--×+×+×



[image: image169.wmf]457

AlV

oofccobcc

Al:MoAlMo

701507.1457

GGG

=-+×+×


	[23]
This work

	Al23V4: 
Model (Al)23(Mo, V)4
	
[image: image170.wmf]234

AlV

oofccobcc

Al:VAlV

383139.09.100234

GTGG

=--×+×+×



[image: image171.wmf]234

AlV

oofccobcc

Al:MoAlMo

435847.736.765234

GTGG

=-+×+×+×


	[23]
This work

	Al3V: 
Model (Al)3(Mo, V)1
	
[image: image172.wmf]3

AlV

oofccobcc

Al:VAlV

95784.20.5203

GTGG

=-+×+×+



[image: image173.wmf]3

AlV

oofccobcc

Al:MoAlMo

129979.436.9443

GTGG

=-+×+×+



[image: image174.wmf]3

AlV

o

Al:Mo,V

8089.97

G

=-


	[23]
This work

This work

	Al8V5: 
Model (Al, V)2(Al, Mo, V)3(Mo, V)2(Al)6
	
[image: image175.wmf]85

AlV

oofccobcc

Al:Al:V:AlAlV

100000112

GGG

=+×+×



[image: image176.wmf]85

AlV

oofccobcc

V:Al:V:AlAlV

528219.926.00094

GTGG

=-×+×+×



[image: image177.wmf]85

AlV

oofccobcc

Al:V:V:AlAlV

454220.026.00085

GTGG

=-+×+×+×



[image: image178.wmf]85

AlV

oofccobcc

V:V:V:AlAlV

26000.067

GGG

=-+×+×



[image: image179.wmf]85

AlV

o

Al,V:Al:V:Al

465244.0

G

=-



[image: image180.wmf]85

AlV

o

Al,V:V:V:Al

465244.0

G

=-



[image: image181.wmf]85

AlV

o

Al:Al,V:V:Al

299767.0

G

=-



[image: image182.wmf]85

AlV

o

V:Al,V:V:Al

299767.0

G

=-



[image: image183.wmf]85

AlV

oofccobcc

Al:Mo:Mo:AlAlMo

85

GGG

=+×+×



[image: image184.wmf]85

AlV

oofccobcc

Al:Al:Mo:AlAlMo

112

GGG

=+×+×



[image: image185.wmf]85

AlV

oofccobccobcc

Al:V:Mo:AlAlMoV

823

GGGG

=+×+×+×



[image: image186.wmf]85

AlV

oofccobccobcc

V:Mo:Mo:AlAlMoV

652

GGGG

=+×+×+×



[image: image187.wmf]85

AlV

oofccobccobcc

V:Mo:V:AlAlMoV

634

GGGG

=+×+×+×



[image: image188.wmf]85

AlV

oofccobccobcc

V:Al:Mo:AlAlMoV

922

GGGG

=+×+×+×



[image: image189.wmf]85

AlV

oofccobccobcc

V:V:Mo:AlAlMoV

625

GGGG

=+×+×+×



[image: image190.wmf]85

AlV

oofccobccobcc

Al:Mo:V:AlAlMoV

420988.667.328832

GTGGG

=-+×+×+×+×



[image: image191.wmf]85

AlV

o

Al:Mo,V:V:Al

147052.5

G

=-


	[23]
[23]
[23]
[23]
[23]
[23]
[23]
[23]
This work

This work

This work

This work

This work

This work

This work

This work

This work


a All parameters are given in J/(mole-atoms); Temperature (T) in K. The Gibbs energies for the pure elements Al, Mo and V are taken from the SGTE database compiled by Dinsdale [21]. 

Table 3 Calculated temperatures for the invariant reactions on the liquidus surface in the Al–Mo–V system compared with the experimental values. 
	Type
	Invariant Reaction
	Temperature, ºC
	Source

	U1
	L + Al63Mo37 ↔ Al8Mo3 + AlMo
	1502
	Calculated (This work)

	U2
	L + AlMo ↔ Al8Mo3 + AlMo3
	1409
	Calculated (This work)

	U3
	L + Al8Mo3 ↔ Al8V5 + AlMo3
	1334
	Calculated (This work)

	E1
	L + (Mo, V) ↔ Al8V5 + AlMo3
L ↔ Al8V5 + AlMo3 + (Mo, V)
	~ 1600
1329
	Measured [27]
Calculated (This work)

	P1
	L + Al8V5 ↔ Al3V + Al8Mo3
L + Al8V5 + Al8Mo3 ↔ Al3V
	~ 1300
1292
	Measured [27]
Calculated (This work)

	U4
	L + Al8Mo3 ↔ Al3V + Al3Mo
	~ 1100
1102
	Measured [27]
Calculated (This work)

	U5
	L + Al3Mo ↔ Al3V + Al4Mo
	1069
	Calculated (This work)

	U6
	L + Al4Mo ↔ Al3V + Al17Mo4
	995
	Calculated (This work)

	U7
	L + Al17Mo4 ↔ Al3V + Al22Mo5
	910
	Calculated (This work)

	P2
	L + Al3V + Al22Mo5 ↔ Al5Mo
	904
	Calculated (This work)

	U8
	L + Al3V ↔ Al6V + Al5Mo

L + Al3V ↔ Al23V4 + Al5Mo
	700

717
	Measured [27]
Calculated (This work)

	U9
	L + Al23V4 ↔ Al45V7 + Al5Mo
	715
	Calculated (This work)

	U10
	L + Al5Mo ↔ Al6V + Al12Mo

L + Al5Mo ↔ Al45V7 + Al12Mo
	690

703
	Measured [27]
Calculated (This work)

	U11
	L + Al6V ↔ Al21V2 + Al12Mo

L + Al45V7 ↔ Al21V2 + Al12Mo
	680

683
	Measured [27]
Calculated (This work)

	U12
	L ↔ Al12Mo + Al21V2 + (Al)

L + Al21V2 ↔ Al12Mo + (Al)
	656

664
	Measured [27]
Calculated (This work)


Figure captions:

Fig. 1 Calculated binary phase diagrams: (a) Al–Mo system [22], (b) Al–V system [23], and (c) Mo–V system [24].

Fig. 2 Observed and calculated isothermal section at 1200 oC of the Al–Mo–V system: (a) observed section by Sperner [27] and (b) calculated section according to the present work along with the experimental data from Sperner [27].
Fig. 3 Calculated isothermal section at 1000 oC of the Al–Mo–V system, compared with the experimental data from Sperner [27] and Raman [28].
Fig. 4 Calculated isothermal section at 750 oC of the Al–Mo–V system, compared with the experimental data from Sperner [27].
Fig. 5 Calculated isothermal section at 715 oC of the Al–Mo–V system, compared with the experimental data from Sperner [27].
Fig. 6 Calculated isothermal sections of the Al–Mo–V system along with the experimental data from Sperner [27]: (a) 675 °C and (b) 630 °C.

Fig. 7 Calculated liquidus surface projection in the Al–Mo–V system: (a) the whole composition, (b) enlarged triangle in (a), and (c) enlarged circle in (b).
Fig. 8 Partial reaction scheme of the Al–Mo–V system according to the present work.
Table captions:

Table 1 Summary of crystal structures of solid phases in the Al–Mo–V system.
Table 2 Summary of the thermodynamic parameters for the Al–Mo–V system.

Table 3 Calculated temperatures for the invariant reactions on the liquidus surface in the Al–Mo–V system compared with the experimental values.
PAGE  
16

_1533473047.unknown

_1544607276.unknown

_1544609535.unknown

_1544610392.unknown

_1544610523.unknown

_1544621405.unknown

_1544622505.unknown

_1544723346.unknown

_1544622506.unknown

_1544622507.unknown

_1544621942.unknown

_1544622257.unknown

_1544622504.unknown

_1544622239.unknown

_1544621890.unknown

_1544621063.unknown

_1544621309.unknown

_1544619955.unknown

_1544610398.unknown

_1544609785.unknown

_1544609995.unknown

_1544610228.unknown

_1544610364.unknown

_1544610188.unknown

_1544609894.unknown

_1544609689.unknown

_1544607537.unknown

_1544609288.unknown

_1544609386.unknown

_1544607686.unknown

_1544607374.unknown

_1544607417.unknown

_1544607332.unknown

_1544594084.unknown

_1544607239.unknown

_1544593953.unknown

_1533492755.unknown

_1544593336.unknown

_1544593360.unknown

_1544593389.unknown

_1544593407.unknown

_1544593952.unknown

_1544593374.unknown

_1544593346.unknown

_1533492757.unknown

_1544593329.unknown

_1533492756.unknown

_1533492753.unknown

_1533492754.unknown

_1533491536.unknown

_1533492752.unknown

_1532961188.unknown

_1533371432.unknown

_1533371980.unknown

_1533472963.unknown

_1533472971.unknown

_1533472952.unknown

_1533371483.unknown

_1533371892.unknown

_1533371471.unknown

_1532961192.unknown

_1532961194.unknown

_1532961193.unknown

_1532961190.unknown

_1532961191.unknown

_1532961189.unknown

_1532961180.unknown

_1532961184.unknown

_1532961186.unknown

_1532961187.unknown

_1532961185.unknown

_1532961182.unknown

_1532961183.unknown

_1532961181.unknown

_1532961172.unknown

_1532961176.unknown

_1532961178.unknown

_1532961179.unknown

_1532961177.unknown

_1532961174.unknown

_1532961175.unknown

_1532961173.unknown

_1532959458.unknown

_1532961170.unknown

_1532961171.unknown

_1532961168.unknown

_1532961169.unknown

_1532961166.unknown

_1532961167.unknown

_1532961165.unknown

_1532959456.unknown

_1532959457.unknown

_1522589726.unknown

_1532863837.unknown

_1532953062.unknown

_1522589722.unknown

