
[image: image1.png]100

‘\_‘—._/0/"

!=;<>f‘_.

g/10g of nodule
——65
—=—4875
——3.25
—=—1.625

—a a5 ——F—#u

40
0.0

0.5 1.0 1.5 2.0

Time. h

2.5



[image: image2.png]ion (%)

Cu ext

100

40

20

g/10g nodule

Time. h

in




[image: image3.png]Ni extraction (%)

100

60

40

,_‘/—_‘—\_‘\‘
VnctS:l

g/10g ofnodule

——65
—8—4875
——325

—m—1625

0.50 1.00 150 2.00

Time. h



[image: image4.png]100

80

60

40 -

Z
S
]

:/.\—.'c‘y"‘

g/10g of nodule

+—65
—=—4875
——325
—=—1625

0.0

=
in

10

-
in

2.0
Time. h

in




[image: image5.png]Fe extraction (%)

100

60

40

20

g/ 10g of nodule
—+—65

0.0

in

10

-
in

Time. h

2.0

in




Figure 1. Effect of amount of hydrazine sulphate under the conditions: P.D 10% (wt/v), H2SO4 2.0% (v/v), temp. 35oC on (a) % Mn extraction, (b) % Cu extraction, (c) % Ni extraction, (d) % Co extraction, and (e) % Fe extraction from mangnaese nodule.
[image: image6.png]Mn extraction (%)

100

60

40

20

T 3]
acid % (v/v)
——3
-2
——172
—=—15
0.0 0.5 Lo 15 2.0

Time. h

in



[image: image7.png]ction (%)

100

60

40

20

acid % (v/v)
—e—3.00

0.0 0. 10 1.

in

in
»
=

Time. h

in




[image: image8.png]Ni extraction (%)

100

60

40

20

/"\‘\0

i,

acid %(v/v)

w

——
—-—2

——172
—=—15

0.0

=
in

Lo L.
Time. h

in

2.0

in



[image: image9.png]ction (%)

100

80 o m— :
60 ——A— A ————
— a0, @ 0 .
40 .
acid %(v/v)
——3
20 M
——172
—=—15
0
0.0 0.5 Lo 15 2.0

Time. h

in




[image: image10.png]Fe extraction (%)

100

80
60
s = @ o
40
acid %(v/v)
——3
20 —-—2
—_——1m
—=—15
0 — —— =" |
0.0 0.5 Lo 15 2.0

Time. h





Figure 2. Effect of H2SO4 concenntration under the conditions: P.D 10%, hydrazine sulphate 3.25 g/10 g of nodule, temp. 35oC on (a) % Mn extraction, (b) % Cu extraction (c) % Ni extraction, (d) % Co extraction, and (e) % Fe extraction from manganese nodule. 

[image: image11.png]——Mn

100

2 2 2
3 3 ]

(95) UOTRENXT [CIRTAL

2
]

120

100

30

60

40

20

Temp.. °C




Figure 3. Effect of temperature on % metal extraction from manganese nodule. Conditions: P.D 10%, hydrazine sulphate 3.25 g/10 g of nodule, time 30 min.

[image: image12.png]g/10g of ore MMO-1
——60
—a—55
—+—50
—a—45

0.0

o

100 150 200 250

Time, (min)





[image: image13.png]Fe extraction (%)

100

60

40

20

g/10g of ore MMO-1
—+—60
1 —8—55
——s0
1 —=—4s
1 - 5 —8— 5 ————+#
A —————
g ———N
0.0 5.0 10.0 15.0 20.0 25.0 30.0 3

Time, (min)

P




Figure 4. Effect of amount of hydrazine sulphate under the conditions: P.D 10% (wt/v), H2SO4 3.0% (v/v), temp. 35oC. on (a) % Mn extraction, and (b) % Fe extraction from MMO-1.
[image: image14.png]Mn extraction (%)

100

60

40

20

L %acid (v/v)

o

i

@
in o

0.0

5.0 10.0 15.0 20.0 25.0 30.0

Time, (min)




[image: image15.png]Fe extraction (%)

100

60

40

20

——4s5
—=—40
——35  %acid (v/v)
1 —=—30
—=—25
—a —a— g—+#
——h— —k —h—
1 — ey — % g
1 -—-——————————— %
0.0 5. 10.0 15.0 20.0 25.0 30.0 3

Time, (min)

P




Figure 5. Effect of H2SO4 concenntration on under the conditions: P.D 10%, hydrazine sulphate 5.5 g/10 g of MMO-1, temp. 35oC on (a) % Mn extraction, and (b) % Fe extraction from MMO-1. 

[image: image16.png]100

w /S__.
60 -
temperature, oC
40 A ——55
—|—45

20 —&—35
0 T T T T T T

0.0 5.0 10.0 15.0 20.0 25.0 30.0

Time, (min)




[image: image17.png]Fe extraction (%)

100

60

40

20

1 temperature, oC
——55
1 - 45
—&—35
1 &  — - A
-~ .
0.0 5.0 10.0 15.0 20.0 25.0 30.0 35.

Time, (min)




Figure 6. Effect of temperature on under the conditions: P.D 10%, H2SO4 3.0% (v/v), hydrazine sulpahte 5.5 g/10 g on (a) % Mn extraction, and (b) % Fe extraction from MMO-1.

[image: image18.png]100

80 4 5 é
60 - g/10g of ore LMO-1
——4.5
40 1 —a—4.0
—A—3.5
20 4 3.0
0
0.0 10.0 20.0 30.0 40.0

Time, (min)




[image: image19.png]g/10g of ore LMO-1

80 ——4.5

—a—4.0

—&—3.5

60 —=-3.0
.—0—0—4/‘
40 % —m a8 — %
F/.__}::>—'+

20

0 T T T T T T

0.0 5.0 10.0 15.0 20.0 25.0 30.0

Time, (min)




Figure 7. Effect of amount of hydrazine sulphate under the conditions: P.D 10% (wt/v), H2SO4 2.5% (v/v), temp. 35oC on (a) % Mn extraction, and (b) % Fe extraction from LMO-1. 

[image: image20.png]100

80 4 l/-/l——l———ll“

60 1 acid %(v/v)
——4.0

10 | —&-3.5
—4—3.0
—-2.5

207 =20

0

0.0 5. 10.0 15.0 20.0 25.0 30.0 3

Time, (min)

P




[image: image21.png]100

20

acid % (v/v)

——4.0
35
——3.0
—-—2.5
——2.0

_
e S—— — ———
-— W N
- iy —— o —e
0.0 5. 10.0 15.0 20.0 25.0 30.0 3

Time, (min)

P




Figure 8. Effect of H2SO4 concentrtaion under the conditions: P.D 10% (wt/v), hydrazine sulphate  3.5% (wt./v), temp. 35oC on (a) % Mn extraction, and (b) % Fe extraction from LMO-1. 

[image: image22.png]Mn extraction (%)

100

60

40

20

g/10 g of LMO-2

——2.00

—=—1.50
——1.00
= 0.50

0.0

o
=
-
=3
=3
-
o

=
»
S
=3
~
DX

=

Time. (min)

w

o





[image: image23.png]Fe extraction (%)

100

60

40

20

g/10g of LMO -2
——2.0
15
——1.0
—&—0.5

5.0 10.0 15.0 20.0 25.0 30.0

Time.(min)




Figure 9. Effect of amount of hydrazine sulphate under the conditions: P.D 10% (wt/v), H2SO4 1.0% (v/v), temp. 35oC on (a) % Mn extraction, and (b) % Fe extraction  from LMO-2. 

[image: image24.png]Mn extraction (%)

100

80

60

40

20

acid %(v/v)

——2.0

5.0

10.0 15.0 20.0

Time,(min)

25.0

30.0

35.0




[image: image25.png]Fe extraction (%)

100

80

60

40

20

——2.0
—-—15
| 1.0 acid%(v/v)
——0.5
-—
- 5 —8— p——+=&
Ak ——h————4
1 -— 5 —S—8—=
0.0 10.0 20.0 30.0

Time, (min)

40.0




Figure 10. Effect of H2SO4 concentrtaion under the conditions: P.D 10% (wt/v), hydrazine sulphate 2.0% (wt./v), temp. 35oC on (a) % Mn extraction, and (b) % Fe extraction from LMO-2. 


















































































(a)





(b)





(c)





(d)





(e)





(a)





(b)





(a)





(b)





(a)





(b)





(a)





(b)





(a)





(b)





(c)





(d)





(e)





(a)





(b)





(a)





(b)





(a)





(b)








1
0
10

