                                                                                                                                                                       Table 1
             Relative dimensional changes of the tested materials as a function of the applied 
          disinfectant and the time since moment of the removal of impressions       
            
	Relative dimensional changes of elastomers - silicones [%] – estimated error limits = 0.025%

	
	30 min
	1 h
	24 h
	7 days

	Material
	Control
	NaOCl

	Sterigum

	Control
	NaOCl
	Sterigum
	Control
	NaOCl
	Sterigum
	Control
	NaOCl
	Sterigum

	1 CS

	0.19
	0.23
	0.14
	0.21
	0.65
	0.44
	0.49
	1.22
	0.65
	0.58
	1.89
	1.11

	2 CS

	0.19
	0.28
	0.20
	0.20
	0.70
	0.42
	0.47
	1.18
	0.67
	0.58
	1.70
	1.21

	3 AS

	0.16
	0.20
	0.12
	0.19
	0.55
	0.33
	0.40
	0.93
	0.58
	0.52
	1.20
	0.85

	4 AS

	0.17
	0.17
	0.10
	0.19
	0.55
	0.30
	0.40
	0.88
	0.49
	0.51
	1.23
	0.78

	Statistics

	Average

	0.178
	0.220
	0.140
	0.198
	0.613
	0.373
	0.440
	1.053
	0.598
	0.548
	1.505
	0.988

	P

	0.073
	0.068
	0.065
	0.066
	0.070
	0.067
	0.060
	0.047
	0.083
	0.043
	0.040
	0.040

	Test value (F)

	2.38
	2.42
	2.55
	2.45
	2.41
	2.42
	2.72
	2.85
	2.25
	2.95
	3.07
	3.12



[image: image1.jpg]



Fig.1 – Measurement - taking photos after disinfection of impressions



[image: image2.jpg]


  [image: image3.jpg]


  [image: image4.jpg]



                   a)                                              b)                                               c) 
Fig.2 – Same cut of two photographies of elastomeric impression: a) immediately after removal, b) 30 min after removal, and (c) differences 




[image: image5.jpg]


  [image: image6.jpg]


  [image: image7.jpg]



                      a)                                              b)                                             c) 
Fig.3 – FFT power spectra of identical cut of two photographies of elastomeric impression:

 a) immediately after removal,  b) 30 min after removal and (c) differences  


[image: image8.wmf]0

1

2

3

4

5

6

7

0.0

0.2

0.4

0.6

0.8

1.0

1.2

1.4

1.6

d [%]

t [day]

 Control

 NaOCl

 Sterigum


 Fig. 4 – Average relative dimensional changes of all the samples as a function of time and  

 applied disinfectant

[image: image9.wmf]0

1

2

3

4

5

6

7

0.0

0.2

0.4

0.6

0.8

1.0

1.2

1.4

1.6

1.8

2.0

d [%]

t [day]

 1 CS Control

 2 CS Control

 1 CS NaOCl

 2 CS NaOCl

 1 CS Sterigum

 2 CS Sterigum


 Fig. 5 – Average relative dimensional changes of the condensation silicones as a function of time and applied disinfectant 

[image: image10.wmf]0

1

2

3

4

5

6

7

0.0

0.2

0.4

0.6

0.8

1.0

1.2

d [%]

t [day]

 3 AS Control

 4 AS Control

 3 AS NaOCl

 4 AS NaOCl

 3 AS Sterigum

 4 AS Sterigum

Fig. 6 – Average relative dimensional changes of addition silicones as a function of time and applied disinfectant 
� NaOCl – 5,25% sodium hypochlorite 


� Sterigum – disinfectant glutaraldehyde and benzalkonium chloride (Zhermack)


� 1CS – condensation silicone Oranwash L (Zhermack)


� 2CS – condensation silicone Xantopren L Blue (Heraeus Kulzer)


� 3AS – addition silicone Elite H-D+ regular body (Zhermack)


� 4AS – addition silicone Flexitime correct flow (Heraeus Kulzer)


� Average –The average values of the ​​obtained mean values ​​of dimensional changes of samples.


� P – The level of significance of the applied test hypotheses compared to the grouped samples for the same applied disinfectant and the same time. 


� Test value - F-value One way ANOVA.





