Mihailo R. Mrdak, Research and Development Center 
IMTEL Communications a. d., Belgrade
Ministarstvo obrazovanja i nauke Republike Srbije
* Acknowledgement: The author is thankful for the financial support from the Ministry of Education and Science of the Republic of Serbia (national project TR 34016).

Razvoj tehnologije izrade obloge i jezgra na bazi domaćih sirovina za proizvodnju specijalnih obloženih elektroda namenjenih za elektrolučno zavarivanje.
TR 34016 Development of technology production cladding and core on based local raw materials for the production of specialty coated electrodes designed for arc welding.
------------------------------

Karakterizacija intermetalne prevlake Cu10tež.%Al naprskane atmosferskim plazma sprej postupkom
OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

Sažetak:
Atmosferski plazma sprej je jedan od postupaka koji se koristi za depoziciju prevlaka otpornih na habanje usled trenja, erozije, kavitacije i korozije. U ovom radu, APS postupkom je proizvedena intermetalna prevlaka Cu10tež.%Al, koja je pouzdani kandidat za primenu u tribološkim okruženjima zbog kombinacije niske cene i izuzetne otpornosti na abraziju pod različitim uslovima rada. Cilj ovoga rada je bio da se izuče mehanička svojstva i struktura intermetalne prvlake Cu10tež.%Al i razvije efikasan metod za reparaciju i poboljšanje otpornosti lakih legura na habanje. Mnoge komponente od legure bakra imaju tendenciju da se degradiraju zbog korozione sredine, trenja, erozije i kavitacije. Takve komponente se mogu spasiti inženjerstvom površina uz primenu odgovarajućih prevlaka na površinama izloženim degradaciji. Tipična mikrostruktura prevlake za APS postupak je lamelarna u kojoj su prisutne mikro pore, neistopljene čestice, među-lamelarni oksidi i precipitati. Mehaničke karakteristike prevlake Cu10tež.%Al ispitane su merenjem mikrotvrdoće slojeva prevlake metodom HV0.3 i čvrstoće spoja metodom ispitivanja na zatezanje. Morfologija čestica praha i površina prevlake analizirana je na skening elektronskom mikroskopu (SEM). Analiza mikrostrukture prevlake je urađena uz korišćenje optičkog mikroskopa, a udeo mikro pora određen je analizom mikrofotografija sa optičkog mikroskopa (OM). 
Ključne reči : atmosfersko plazma prskanje, intermetalna prevlaka, bakar - aluminijum, mikrotvrdoća, čvrstoća spoja.

Characterization of intermetallic coating Cu10wt.% Al sprayed atmospheric plasma spraying
FIELD: Chemical Technology

ARTICLE  TYPE: Original Scientific Paper

Summary:

Atmospheric plasma spray is one of the procedures used for deposition of coatings resistant to wear caused by abrasion, erosion, cavitation and corrosion. n this paper, APS procedure produced intermetallic coating Cu10wt.% Al, which is a reliable candidate for use in tribological environments due to a combination of low price and outstanding abrasion resistance under different conditions. The aim of this study was to investigate the mechanical properties and structure of the intermetallic prvlake Cu10wt.% Al and develop an efficient method for repairing and improving resistance alloy wear. Many components of the alloys tend to degrade the corrosion protection, friction, erosion and cavitation. Such components can be engineered to save space using appropriate coatings on surfaces exposed to degradation. Typical microstructures coating of APS process is lamellar in which present the micro pores, unmelted particles, inter-lamellar oxides and precipitates. Mechanical properties of coatings Cu10wt.% Al were investigated by measuring the microhardness of layers of coating method HV0.3 and bond strength test method of tightening. The morphology of the powder particles and the surface coatings was analyzed by the scanning electron microscope (SEM). Analysis of the microstructure of the coating is done with the use of an optical microscope, and the proportion of pores is determined by analyzing the micrographs of the optical microscope (OM).
Key words: atmospheric plasma spraying, intermetallic coating, copper - aluminum, the microhardness and bond strength
LITERATURE 

ASM Handbook, 1992, Volume 3, Alloy Phase Diagrams, ASM International, Metals Park.

Altuncu, E., Iriç, S., Ustel, F., 2012, Wear – resistant intermetallic arc spray coatings, Materiali in tehnologije / Materials and technology, 46(2), pp.181–183.
Bartuli, C., Valent, T., Casadei, F., Tului, M., 2007, Advanced thermal spray coatings for tribological applications, Proceedings of the Institution of Mechanical Engineers, Part L: Journal of Materials:Design and Applications, 221, pp.175–185.

Hang, C.J., Wang, C.Q., Mayer, M., Tian, Y.H., Zhou, Y., Wang, H.H., 2008, Growth Behavior of Cu/Al Intermetallic Compounds and Cracks in Copper Ball Bonds during Isothermal Aging, Microelectronics Reliability 48, pp.416-424.

Li, C., Sun, B., 2004, Microstructure and Property of micro-plasma-sprayed Cu coating, Materials Science and Engineering A 379, pp.92-101.

Limpichaipanit, A., Watcharapasorn, A., Wirojanupatump, S., Jiansirisomboon, S., 2011, Fabrication and Mechanical Properties of Thermal Sprayed Copper-based Coatings, Journal of the Microscopy Society of Thailand, 4(2), pp.123-126.
Material Product Data Sheet, 2012, Aluminum Bronze Thermal Spray Powders Thermal Spray Powder Products Metco 445, DSMTS-0103.0, Sulzer Metco.

Mihailo Mrdak, Marko Rakin, Bojan Medjo, Nikola Bajić, 2015, Experimental Study of Insulating Properties and Behaviour of Thermal Barrier Coating Systems in Thermo Cyclic Conditions Materials and Design, Materials and Design, 67, pp.337-343.
Мrdak, М., 2015, Characteristics of APS and VPS plasma spray processes, Vojnotehnički glasnik/Military Technical Courier, 63(3), pp.137-159.
Mrdak M., 2015, Morphology of powder particles produced by spray atomization and other processes, Vojnotehnički glasnik/ MilitaryTechnical Courier, 63(4), pp.46-67.
Mrdak, М., 2016, Study of the application of plasma sprayed coatings on the sections of the Astazou III B turbo - jet engine, Vojnotehnički glasnik / Military Technical Courier, 64(1), pp.1-25.

Mrdak, M., 2016, Properties of the ZrO2MgO/MgZrO3NiCr/NiCr triple-layer thermal barrier coating deposited by the atmospheric plasma spray process, Vojnotehnički glasnik / Military Technical Coуrier, 64(2), pp.411-430.
Sartale, S.D., Yoshitake, M., 2010, Investigation of Cu–Al surface alloy formation on Cu substrate, Journal of Vacuum Science & Technology B, 28, pp.353–360.

Turbojet Engine – Standard Practices Manual (PN 582005), 2002, Pratt & Whitney, East Hartford, USA.
Vencl, A., Arostegui, S., Favaro, G., Zivic, F., Mrdak, M., Mitrović, S., Popovic, V., 2011, Evaluation of adhesion/cohesion bond strength of the thick plasma spray coatings by scratch testing on coatings cross-sections, Tribology International, 44(11), pp.1281-1288.
Vencl, A., Manić, N., Popovic, V., Mrdak, M., 2010, Possibility of the abrasive wear resistance determination with scratch tester, Tribology Letters, 37(3), pp.591-604.
Wang, B.Q., Seitz, M.W., 2001, Comparison in erosion behavior of ironbase coatings sprayed by three different arc-spray processes, Wear, 250, pp.755–761.

Zhang, Z., Li, D., Wang, S., 2006, High Temperature Performance of Arc-sprayed Aluminium Bronze Coatings for Steel, Transactions of Nonferrous Metals Society of China 16, pp.868-872.
