Propratno pismo za dostavljeni članak
Članak koji vam dostavljen odnosi se na naučni rad u kojem su izneti prethodno neobjavljeni rezultati sopstvenih istraživanja. Sve prikazane slike su originali.

Struktura i svojstva prevlake Ni22Cr10Al1Y deponovane vakuum plazma sprej procesom
OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

JEZIK ČLANKA: engleski

Sažetak:
U ovome radu, cilj je bio da se vakuum plazma sprej procesom deponuju slojevi prevlake Ni22Cr10Al1Y za zaštitu komponenti gasnih turbina od oksidacije i visokotemperaturne korozije. Prevlaka može znatno uticati na svojstva substrata jer zajedno sa substratom formira kompozit. Vrsta procesa depozicije prevlake i režim termičke obrade prevlake sa substratom bitno utiču na njenu otpornost na visokotemperaturno puzanje. Deponovanje praha Ni22Cr10Al1Y urađeno je sa vakuum plazma sprej sistemom firme Plasma Technik - AG koji koristi komandni pult A-2000 i plazma pištoljem F4. Prevlaka deponovana na substratu od legure INCONEL X-750 termički je obrađena na 11000C u trajanju od 2 sata u zaštitnoj atmosferi argona. Morfologija čestica praha ispitana je metodom skening elektronske mikroskopije. Ispitivanja mikrotvrdoće slojeva rađena su metodom HV0.3 i čvrstoće spoja metodom ispitivanja na zatezanje, koja su bila u skladu sa standardom Pratt & Whitney. Mikrostruktura slojeva prevlake u deponovanom stanju ispitana je na svetlosnom mikroskopu. Nagrizanje prevlake rađeno je mešanjem azotne kiseline 2.5ml HNO3 sa 7.5ml fluorovodonične kiseline HF. Analiza mikrostrukture nagrizene prevlake pre i posle termičke obrade, kao i debljina difuzione zone izvedena je na svetlosnom mikroskopu, na osnovu čega se dala ocena kvaliteta prevlake.

Ključne reči: VPS - vakuum plazma sprej proces, Ni22Cr10A1Y, mikrostruktura, interfejs, mikrotvrdoća, čvrstoća spoja.
Structure and properties of Ni22Cr10Al1Y coatings deposited by vacuum plasma spray process

FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

ARTICLE LANGUAGE: English 

Summary:

In this study, the aim was to vacuum plasma spray process of depositing layers of coating Ni22Cr10Al1Y to protect gas turbine engine components from oxidation and high-temperature corrosion.The coating can significantly affect on the properties of the substrate because of together with the substrate forming a composite. Type deposition coating process and heat treatment of the coating with the substrate essentially affect its resistance to high temperature creep. Depositing powder Ni22Cr10Al1Y done with a vacuum plasma spray system company Plasma Technik - AG using control panel A-2000 and the plasma gun F4. Coating deposited on a substrate of INCONEL Alloy X-750 were thermally treated at 1100ºC for 2 hours in a protective atmosphere of argon. Particle morphology was tested by scanning electron microscopy.Tests microhardness of layers made by the method HV0.3 and bond strength test method to tension, which were in accordance with standard Pratt & Whitney. The microstructure of the deposited layers of coating condition was examined under a light microscope. Corrosion coating is done by mixing nitric acid a 2.5ml HNO3 with 7.5ml hydrofluoric acid HF. Analysis of microstructure etched coating before and after heat treatment, as well as the thickness of the diffusion zone is carried out under a light microscope, based on the assessment made by the quality of the coating.
Keywords:VPS - vacuum plasma spray process, Ni22Cr10A1Y, microstructure, interface, micro-hardness, bond strength

Podaci o autoru: 

Mihailo R.Mrdak ,doktor tehničkih nauka sa zvanjem naučnog saradnika .Radio od 1987 -2008.god u VZ "Moma Stanojlović"na poslovima načelnika odelenja plazme i vodećeg istraživača. Sada radi u institutu IMTEL. na projektima Ministarstva prosvete nauke i tehnološkog razvoja sa naučnim zvanjem viši naučni saradnik.
E – mail :
drmrdakmihailoi@insimtel.com
Adresa na poslu:

Istraživački razvojni centar IMTEL Komunikacije a. d., Belgrade 

Bulevar M.Pupina 165b,11070 N.Beograd.

Adresa kući:

Mihailo R. Mrdak
Braće Burgerovih 10/1

11185 Zemun Polje

Telefoni:
011 – 3757 – 632
064 – 264 - 8332

Matični broj:
2201957260015 
Tekući račun je otvoren kod Poštanske štedionice  200  4220099  68







