Propratno pismo za dostavljeni članak
Članak koji vam dostavljen odnosi se na naučni rad u kojem su izneti prethodno neobjavljeni rezultati sopstvenih istraživanja. Sve prikazane slike su originali.

Svojstva prevlake deponovane sa difuziono oksidiranim prahom Mo&O2 primenom APS procesa
ORCID iD: 


http://orcid.org/0000-0003-3983-1605
OBLAST: Hemijske tehnologije

TIP ČLANKA: Izvorni naučni rad

Sažetak:
Prah Mo&O2 ima značajnu ulogu za proizvodnju prevlaka sa povišenom otpornošću na klizanje u uslovima bez primene maziva. Prevlake Mo&O2 imaju mali koeficijent frikcije i dobre karakteristike na habanje pri mehaničkim naprezanjima. U cilju proizvodnje prevlaka visoke tvrdoće, prah Mo&O2 je deponovan plazmom sa optimalnim parametrima. Karakterizacija oblika površine čestica oksidnog praha i površine preloma prevlake izvedena je metodom SEM, a mikrostruktura slojeva primenom svetlosne mikroskopije. Mikrostruktura prevlake se sastoji od lamela Mo i tankih filmova primarnih oksida MoO2 i MoO3 koje okružuju lamele Mo. Analiza dobijenih rezultata pokazala je da slojevi prevlake Mo&O2 sa difuziono oksidiranim česticama Mo imaju strukturu i mehaničke karakteristike, koje omogućuju njenu primenu na površinama radnih delova u uslovima habanja i klizanja trenjem bez maziva.

Ključne reči: Mo&O2, prevlaka, mikrostruktura, mehaničke karakteristike

Properties of the coating deposited with diffusion of oxidized powder Mo&O2 using aps process

ORCID iD: 

http://orcid.org/0000-0003-3983-1605
FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

ARTICLE LANGUAGE: English 

Summary:

Powder Mo&O2 has an important role for the production of coatings with increased resistance to slide in conditions without the use of lubricants. Mo&O2. Coatings have low coefficient of friction and good abrasion characteristics in mechanical stresses. In aim to produce coatings of high hardness, powder Mo&O2 is plasma deposited with optimal parameters. Characterization of the surface shape of the particles of the oxide powder and the fracture surface coating is performed by SEM, a microstructure layers by using light microscopy. The microstructure of the coating consists of a lamellae Mo i primary oxide thin film MoO3 and MoO2, which surrounding the lamellae Mo. Analysis of the obtained results showed that the coating layers of Mo&O2 with the diffusion oxidized Mo particles have a structure and mechanical characteristics, which enable its application in areas of working parts in terms of wear and sliding friction without lubricant.

Keywords: Mo&O2, coatings, microstructure, mechanical properties

Podaci o autoru: 

Mihailo R.Mrdak ,doktor tehničkih nauka sa zvanjem naučnog saradnika .Radio od 1987 -2008.god u VZ "Moma Stanojlović"na poslovima načelnika odelenja plazme i vodećeg istraživača. Sada radi u institutu IMTEL. na projektima Ministarstva prosvete nauke i tehnološkog razvoja sa naučnim zvanjem viši naučni saradnik.
E – mail :
drmrdakmihailoi@insimtel.com
Adresa na poslu:

Istraživački razvojni centar IMTEL Komunikacije a. d., Belgrade 

Bulevar M.Pupina 165b,11070 N.Beograd.

Adresa kući:

Mihailo R. Mrdak
Braće Burgerovih 10/1

11185 Zemun Polje

Telefoni:
011 – 3757 – 632
064 – 264 - 8332

Matični broj:
2201957260015 
Tekući račun je otvoren kod Poštanske štedionice  200  4220099  68







