Mihailo R. Mrdak, Research and Development Center 
IMTEL Communications a. d., Belgrade 
Ministarstvo obrazovanja nauke i tehnološkog razvoja Republike Srbije
* Acknowledgement: The author is thankful for the financial support from the Ministry of Education Science and technological development of the Republic of Serbia (national projects OI 174004). 
Mikromehanički kriterijumi oštećenja i loma biomedicinskih implanata od lergura titana, kobalta i aluminijuma. 
OI 174004  Micromechanical criteria of damage and fracture of biomedical implants of alloys titanium, cobalt and aluminum.
Ispitivanje mehaničko strukturnih karakteristika oksidne keramike Al2O3 otporne na trenje klizanjem
OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

Sažetak:
Al2O3  je tvrda oksidna keramika hemijski bioinertna sa dobrim kliznim svojstvima, koja je našla široku primenu u projektovanju inženjerskih komponenti. Cilj rada bio je da se APS procesom sa promenom plazma struje proizvedu slojevi Al2O3 strukturnih i mehaničkih karakteristika koji će naći primenu za proizvodnju biomedicinskih prevlaka zasebno ili u kombinaciji sa hidroksiapatom (HA) na površinama legura koje se koriste za izradu implanata. Prevlaka je deponovana sa plazma strujom 700, 800 i 900A. Mehaničke karakteristike prevlake ispitane su primenom standarda Pratt & Whitney. Oblik površine čestica praha i površina prevlake ispitana je metodom SEM. Metalografska analiza unutrašnjih slojeva ispitana je svetlosnom mikroskopijom. Najbolje strukturne i mehaničke karakteristike Al2O3 prevlake deponovane sa 900A potvrđene su ispitivanjem kliznih svojstava prevlake deponovne i polirane do ogledala na zaptivnom prstenu uparenim sa grafitnim prstenom na vodenoj kočnici.
Ključne reči: Keramika, mehaničke karakteristike, struktura, habanje klizanjem.
Testing of mechanical structural characteristics oxide ceramics Al2O3 resistant on sliding friction
FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

Summary:

Al2O3 is hard oxide ceramic chemical bio inert with good sliding properties, which has found wide use in the design of engineering components. The aim was to APS process with the change of plasma currents produce Al2O3 layers of structural and mechanical properties which will find application in the manufacture of biomedical coatings alone or in combination with hydroxyapatite (HA) on the surfaces of the alloy used for making implants. The coating was deposited with a plasma current of 700, 800 and 900 A. Mechanical properties of coatings were tested using the standard Pratt & Whitney. The shape of the surface of the powder particles and the surface coating was tested by SEM. Metallographic analysis of the inner layers was examined by light microscopy. The best structural and mechanical properties of Al2O3 coatings deposited with the 900A were confirmed by testing sliding properties of the coating deposition and polished to a mirror on the sealing ring paired with graphite ring on water brake. 
Keywords: ceramics, mechanical properties, structure, sliding abrasion
References
Friis, M., Persson, C., Wigren, J., 2001, Influence of particle in-flight characteristics on the microstructure of atmospheric plasma sprayed yttria stabilized ZrO2, Surface and Coatings Technology, 141(2-3), pp.115-127.

Gadow, R., Killinger, A., Stiegler, N., 2010, Hydroxyapatite coatings for biomedical applications deposited by different thermal spray techniques, Surface and Coatings Technology, pp.1157-1164.

Hsiung, J.C., Kung, H.K., Chen, H.S., Chang, K.Y., 2012, Applications of Thermal Spray Coating in Artificial Knee Joints, Life Science Journal, 9(1), pp.457-463.

Kulkarni, A., Gutleber, J., Sampath, S., Goland, A., Lindquist, W.B., Herman, H., Allen, A.J., Dowd, B., 2004, Studies of the microstructure and peoperties of dense ceramic coatings produced by high-velocity oxygen-fuel combustion spraying, Materials Science and Engineering A369, pp.124-137.

Li, C.J., Ohmori, A., 2002, Relationship between the structure and properties of thermally sprayed coatings, Journal of Thermal Spray Technology, 11, pp.365-374.

Li, C.J, Yang, G.J,  Ohmori, A., 2006, Relationship between particle erosion and lamellar microstructure for plasma-sprayed alumina coatings, Wear, 200, pp.1166-1172. 

Liao, H.,  Normand, B., Coddet, C., 2000, Influence of coating microstructure on the abrasive wear resistance of WC/Co cermet coatings, Surface and Coatings Technology, 124, pp.235-242.

Liou, S., 2009, Biomedical Titanium Alloys and Surface Modification, Chemical Industry.

Material Product Data Sheet, 2012, Metco 105NS Aluminum Oxide Thermal Spray Powders, DSMTS-0005.1, Sulzer Metco.

Matejicek, J., Sampath, S., 2001, Intrinsic Residual Stresses in Single Splats Produced by Thermal Spray Processes, Acta Materialia, 49, pp.1993-1999.

Mrdak, М., 2016, Study of the application of plasma sprayed coatings on the sections of the Astazou III B turbo - jet engine, Vojnotehnički glasnik / Military Technical Courier, 64(1), pp.1-25.

Mrdak, M., 2016, Properties of the ZrO2MgO/MgZrO3NiCr/NiCr triple-layer thermal barrier coating deposited by the atmospheric plasma spray process, Vojnotehnički glasnik / Military Technical Coуrier, 64(2), pp.411-430.

Toma, D., Brandl, W., Marginean, G., 2001, Wear and corrosion resistance of thermally sprayed cermet coatings, Surface and Coatings Technology, 138, pp.149-158. 
Tucker, R.C., 2002, Thermal spray coatings: broad and growing applications, International Journal of Powder Metallurgy, 38, pp.45–53.

Turbojet Engine – Standard Practices Manual (PN 582005), 2002, Pratt & Whitney, East Hartford, USA.
Yang, H., Luan, W. and Tu, S-T, 2006, Corrosion Behavior and Thermal Conductivity of Plasma Sprayed AlN/Al2O3 Coating, Materials Transactions, 47(7), pp.1649-1653.
