Propratno pismo za dostavljeni članak
Članak koji vam dostavljen odnosi se na naučni rad u kojem su izneti prethodno neobjavljeni rezultati sopstvenih istraživanja. Sve prikazane slike su originali.

Mehanička svojstva i mikrostrukture bioinertnih slojeva hrom oksidnih prevlaka deponovanih APS - procesom
OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

Sažetak:
Plazma sprej keramički slojevi Cr2O3 koriste se kao zasebna prevlaka ili kao dodatak bioreaktivnoj organskoj kompozitnoj keramici Ca10(PO4)6(OH)2-Al2O3-ZrO2-Cr2O3 i drugim bioinertnim keramikama praveći kompozi tipa Al2O3–ZrO2–SrO–Cr2O3–Y2O3, ZrO2-TiO2-Cr2O3 i TiO2-Cr2O3 za povećanje mehaničkih karakteristika i otpornosti komponenti veštačkog zgloba na habanje klizanjem i koroziju. U radu je analiziran uticaj odstojanja plazma pištolja od podloge na mehaničke karakteristike i mikrostrukturu Cr2O3 slojeva deponovanih sa snagom napajanja od 40kW. Cilj rada je bio da se deponuju slojevi optimalnih karakteristika koji će omogućiti efikasnu primenu Cr2O3 slojeva na podlogama čeličnih implantata izloženih suvom trenju bez podmazivanja i koroziji živih tkiva. Ispitivanje mehaničkih karakteristika realizovano je ispitivanjem mikrotvrdoće slojeva metodom HV0.3 i čvrstoće spoja metodom na zatezanje. Izgled površine čestica praha ispitan je metodom SEM. Mikrostrukture slojeva su analizirane uz primenu optičkog mikroskopa (OM) i skening elektronskog mikroskopa (SEM). Rezultati ispitivanja potvrdili su mogućnost efikasne primene bioinertnih slojeva Cr2O3  sa drugim keramikama namenjenih za izradu funkcionalnih implantatima.

Ključne reči: plazma prskanje, Cr2O3, implantati, mikrotvrdoća, čvrstoća spoja.
Mechanical properties and microstructure bio-inert layer chrome oxide coatings deposited APS - process
FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

Summary:

Plasma Spray Cr2O3 ceramic layers are used as a separate coating or as a supplement bio-reactive organic composite ceramics Ca10(PO4)6(OH)2-Al2O3-ZrO2-Cr2O3 and other bio-inert ceramics making composing type Al2O3–ZrO2–SrO–Cr2O3–Y2O3, ZrO2-TiO2-Cr2O3 and TiO2-Cr2O3 to increase the mechanical properties and resistance components of artificial joint on sliding abrasion and corrosion. This paper analyzes the influence of the plasma gun distance from the substrate to the mechanical properties and microstructure of Cr2O3 layers deposited with the power of 40kW power. The aim was to deposit layers with optimal characteristics that will enable the effective implementation Cr2O3 layers on substrates of steel implants exposed dry friction without lubrication and corrosion living tissue. Testing of mechanical properties was implemented by examining microhardness layers method HV0.3 and strength of the tightening method. The appearance of the surface of the powder particles was tested method of SEM. Microstructure layers were analyzed with the use of an optical microscope (OM) and scanning electron microscope (SEM). Test results confirmed the possibility of effective application of bio-inert layers of Cr2O3 with other ceramics intended for the production of functional implants.

Keywords: plasma spraying, Cr2O3, implants, microhardness, bond strength. 
Podaci o autoru: 

Mihailo R.Mrdak ,doktor tehničkih nauka sa zvanjem naučnog saradnika .Radio od 1987 -2008.god u VZ "Moma Stanojlović"na poslovima načelnika odelenja plazme i vodećeg istraživača. Sada radi u institutu IMTEL. na projektima Ministarstva prosvete nauke i tehnološkog razvoja sa naučnim zvanjem viši naučni saradnik.
E – mail :
 drmrdakmihailoi@insimtel.com
Adresa na poslu:

Istraživački razvojni centar IMTEL Komunikacije a. d., Belgrade 

Bulevar M.Pupina 165b,11070 N.Beograd.

Adresa kući:

Mihailo R. Mrdak
Braće Burgerovih 10/1

11185 Zemun Polje

Telefoni:
011 – 3757 – 632 , 064 – 264 - 8332

Matični broj:
2201957260015 
Tekući račun je otvoren kod Poštanske štedionice  200  4220099  68







