Propratno pismo za dostavljeni članak
Članak koji vam dostavljen odnosi se na naučni rad u kojem su izneti prethodno neobjavljeni rezultati sopstvenih istraživanja u VZ " Moma Stanojlović"Batajnica.Sve prikazane slike su originali.

Mehanička svojstva i metalografska analiza plazma sprej APS - Ni - 5.5 tež.% Al - 5 tež.% Mo prevlake 

OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

Sažetak:
U ovom radu predstavljena su ispitivanja mehaničkih i mikrostrukturnih karakteristika atmosferski plazma sprej (APS) prevlaka od kompozitnog praha Ni - 5,5tež.%Al - 5 tež.% Mo. Cilj istraživanja je bio da se optimizuje protok praha (g/min) kako bi se deponovali slojevi NiAlMo prevlake optimalnih mehaničkih i strukturnih karakteristika koji će se primeniti na pohabanim vazduhoplovnim delovima od legura Ni izloženi kombinaciji korozije i habanja. Mikrotvrdoće deponovanih slojeva su urađene metodom HV0.3 i zatezna čvrstoće spoja metodom ispitivanja na zatezanje. Morfologija površine čestica praha ispitana je na SEM-u (skening elektronskom mikroskopu). Mikrostruktura NiAlMo prevlaka je ispitana na optičkom mikroskopu (OM).Morfologija loma najboljih slojeva je ispitana na skening elektonskom mikroskopu (SEM). Utvrđeno je da se sa kontrolom protoka praha mogu proizvesti  slojevi prevlake sa dobrom čvrstoćom spoja.

Ključne reči: Atmosferski plazma sprej (APS), mikrostruktura, Ni-5,5wt.%Al-5wt.%Mo, mikrotvrdoća, čvrstoća spoja. 

Mechanical properties and metallographic analysis of plasma spray APS - Ni - 5.5 wt.% Al - 5 wt.% Mo coatings

FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

Summary:

In this paper presented the testing of mechanical and microstructural characteristics of the atmospheric plasma spray (APS) coatings of composite powder Ni - 5.5 wt.% Al - 5 wt.% Mo. The aim of this study was to optimize the flow of powder (g / min) in order to deposit the layers NiAlMo coating optimum mechanical and structural characteristics which will be applied to the worn aviation parts of alloy Ni exposed to a combination of corrosion and wear. Microhardness of the deposited layers were made using HV0.3 and tensile bond strength test method tensile. The morphology of the powder particles was examined in SEM (scanning electron microscope). NiAlMo coating microstructure was examined on an optical microscope (OM). Fracture morphology of the top layer has been tested on an electronic scanning microscope (SEM). It was found that the control flow of powder coatings can produce coatings with good strength circuit.

Key words: atmospheric plasma spraying (APS), Ni-5.5wt.%Al- 5 wt.%Mo, microhardness, bond strength.

Podaci o autoru: 

Mihailo R.Mrdak ,doktor tehničkih nauka sa zvanjem naučnog saradnika .Radio od 1987 -2008.god u VZ "Moma Stanojlović"na poslovima načelnika odelenja plazme i vodećeg istraživača.Od 2008.god. radi u institutu IMTEL.

E – mail :
 miki@insimtel.com
Adresa na poslu:

Istraživački razvojni centar IMTEL Komunikacije a. d., Belgrade 

Bulevar M.Pupina 165b,11070 N.Beograd.

Adresa kući:

Mihailo R. Mrdak
Braće Burgerovih 10/1

11185 Zemun Polje

Telefoni:
011 – 3757 – 632 , 064 – 264 - 8332

Matični broj:
2201957260015 
Tekući račun je otvoren kod Poštanske štedionice  200  4220099  68







