Mihailo R. Mrdak, Research and Development Center 
IMTEL Communications a. d., Belgrade 
Ministarstvo obrazovanja nauke i tehnološkog razvoja Republike Srbije
* Acknowledgement: The author is thankful for the financial support from the Ministry of Education and Science of the Republic of Serbia (national project TR 34016). TR 34016
Razvoj tehnologije izrade obloge i jezgra na bazi domaćih sirovina za proizvodnju specijalnih obloženih elektroda namenjenih za elektrolučno zavarivanje.
Development of technology production cladding and core on based local raw materials for the production of specialty coated electrodes designed for arc welding.

Struktura i svojstva prevlake Ni22Cr10Al1Y deponovane vakuum plazma sprej procesom
OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

JEZIK ČLANKA: engleski

Sažetak:
U ovome radu, cilj je bio da se vakuum plazma sprej procesom deponuju slojevi prevlake Ni22Cr10Al1Y za zaštitu komponenti gasnih turbina od oksidacije i visokotemperaturne korozije. Prevlaka može znatno uticati na svojstva substrata jer zajedno sa substratom formira kompozit. Vrsta procesa depozicije prevlake i režim termičke obrade prevlake sa substratom bitno utiču na njenu otpornost na visokotemperaturno puzanje. Deponovanje praha Ni22Cr10Al1Y urađeno je sa vakuum plazma sprej sistemom firme Plasma Technik - AG koji koristi komandni pult A-2000 i plazma pištoljem F4. Prevlaka deponovana na substratu od legure INCONEL X-750 termički je obrađena na 11000C u trajanju od 2 sata u zaštitnoj atmosferi argona. Morfologija čestica praha ispitana je metodom skening elektronske mikroskopije. Ispitivanja mikrotvrdoće slojeva rađena su metodom HV0.3 i čvrstoće spoja metodom ispitivanja na zatezanje, koja su bila u skladu sa standardom Pratt & Whitney. Mikrostruktura slojeva prevlake u deponovanom stanju ispitana je na svetlosnom mikroskopu. Nagrizanje prevlake rađeno je mešanjem azotne kiseline 2.5ml HNO3 sa 7.5ml fluorovodonične kiseline HF. Analiza mikrostrukture nagrizene prevlake pre i posle termičke obrade, kao i debljina difuzione zone izvedena je na svetlosnom mikroskopu, na osnovu čega se dala ocena kvaliteta prevlake.

Ključne reči: VPS - vakuum plazma sprej proces, Ni22Cr10A1Y, mikrostruktura, interfejs, mikrotvrdoća, čvrstoća spoja.
Structure and properties of Ni22Cr10Al1Y coatings deposited by vacuum plasma spray process

FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

ARTICLE LANGUAGE: English 

Summary:

In this study, the aim was to vacuum plasma spray process of depositing layers of coating Ni22Cr10Al1Y to protect gas turbine engine components from oxidation and high-temperature corrosion.The coating can significantly affect on the properties of the substrate because of together with the substrate forming a composite. Type deposition coating process and heat treatment of the coating with the substrate essentially affect its resistance to high temperature creep. Depositing powder Ni22Cr10Al1Y done with a vacuum plasma spray system company Plasma Technik - AG using control panel A-2000 and the plasma gun F4. Coating deposited on a substrate of INCONEL Alloy X-750 were thermally treated at 1100ºC for 2 hours in a protective atmosphere of argon. Particle morphology was tested by scanning electron microscopy.Tests microhardness of layers made by the method HV0.3 and bond strength test method to tension, which were in accordance with standard Pratt & Whitney. The microstructure of the deposited layers of coating condition was examined under a light microscope. Corrosion coating is done by mixing nitric acid a 2.5ml HNO3 with 7.5ml hydrofluoric acid HF. Analysis of microstructure etched coating before and after heat treatment, as well as the thickness of the diffusion zone is carried out under a light microscope, based on the assessment made by the quality of the coating.
Keywords:VPS - vacuum plasma spray process, Ni22Cr10A1Y, microstructure, interface, micro-hardness, bond strength

References
Achar, D.R.G., Munoz-Arroyo, R., Singheiser, L. and Quadakkers, W.J., 2004, Modelling of phase equilibria in MCrAlY coating systems, Surface and Coatings Technology, 187(2–3), pp. 272–283.
Feuerstein, A., Knapp, J., Taylor, T., Ashary, A., Bolcavage, A., Hitchman, N., 2008, Technical and Economical Aspects of Current Thermal Barrier Coating Systems for Gas Turbine Engines by Thermal Spray and EBPVD: A Review. Journal of Thermal Spray Technology, 17(2), pp.199-213.

Funk, M., Ma, K., Eberl, C., Schoenung, J.M., Göken, M. and Hemer, K.J., 2011, High-Temperature Mechanical Behavior of End-of-Life Cryomilled NiCrAlY Bond Coat Materials, Metallurgical and materials transactions A, 42A, pp.2233-2241.
Gómez-Acebo, T., Navarcorena, B., Castro, F., 2004, Interdiffusion in multiphase, Al-Co-Cr-Ni-Ti diffusion couples, Journal of Phase Equilibria and Diffusion, 25(3), pp.237-251.
Hald, J. and Horsewell, A., 2006, Interdiffusion between Ni-based superalloy and MCrAlY coating , Defect and Diffusion Forum, 258-260, pp.73-78.

Itoh, Y. and Tamura, M., 1999, Reaction Diffusion Behaviors for Interface Between Ni-Based Super Alloys and Vacuum Plasma Sprayed MCrAlY Coatings, Journal of Engineering for Gas Turbines and Power, 121, pp.476 – 483.
Ma, K., Tang, F. and Schoenung, J.M., 2010, Investigation into the effects of Fe additions on the equilibrium phase compositions, phase fractions and phase stabilities in the Ni–Cr–Al system, Acta Materialia, 58(5), pp.1518–1529.
Material Product Data Sheet, 2012, Nickel Chromium Aluminum Yttrium (NiCrAlY) Thermal Spray Powders, Amdry 9624, DSMTS-0102.0, Sulzer Metco.
Mendis, B.G. and Hemker, K.J., 2008, Thermal stability of microstructural phases in commercial NiCoCrAlY bond coats, Scripta Materialia, 58(4), pp.255–258.
Mrdak, M., 2012, Plasma deposited layers of nickel-chrome-aluminum-yttrium coatings resistant to oxidation and hot corrosion, Vojnotehnički glasnik/Military Technical Courier, 60(2), pp.182-201.
Mrdak, M., 2013, Characterization of vacuum plasma sprayed cobalt-nickel-chromium-aluminum-yttrium coating, Vojnotehnički glasnik/Military Technical Courier, 61(4), pp.26-47.
Mihailo Mrdak1, Marko Rakin 2, Bojan Medjo 2, Nikola Bajić 3, 2015, Experimental Study of Insulating Properties and Behaviour of Thermal Barrier Coating Systems in Thermo Cyclic Conditions, Materials & Design, 67, pp.337-343.
Mrdak, М., 2016, Study of the application of plasma sprayed coatings on the sections of the Astazou III B turbo - jet engine, Vojnotehnički glasnik/Military Technical Courier, 64(1), pp.1-25. 
Padture, N.P., Gell, M. and Jordan, E.H., 2002, Thermal barrier coatings for gas-turbine engine applications, Science, 296 (5566), pp.280–284.
Tang, F., Ajdelsztajn, L., Kim, G.E., Provenzano, V. and Schoenung, J.M., 2006, Effects of variations in coating materials and process conditions on thethermal cycle properties of NiCrAlY/YSZ thermal barrier coatings, Materials Science and Engineering A, 425(1-2), pp.94–106.
Turbojet Engine – Standard Practices Manual PN 582005, 2002, Pratt & Whitney, East Hartford, USA.

Wang, B., Gong, J., Wang, A.Y., Sun, C., Huang, R.F. and Wen, L.S., 2002, Oxidation behavior of NiCrAlY coatings on Ni based superalloy, Surface and Coatings Technology, 149, p.70.

Liu, Y.Z., Hu, X.B., Zheng, S.J., Zhu, Y.L., Wei, H., Ma, X.L., 2015, Microstructural evolution of the interface between NiCrAlY coating and superalloy during isothermal oxidation, Materials and Design 80, pp. 63–69.

Yuan, K., Eriksson, R., Lin Peng, R., Li, X., Johansson, S., Wang, Y., 2014, MCrAlY coating design based on oxidation - diffusion modelling. Part I: Microstructural evolution, Surface and Coatings Technology 254, pp.79- 96.
