Mihailo R. Mrdak, Research and Development Center 
IMTEL Communications a. d., Belgrade 
Ministarstvo obrazovanja nauke i tehnološkog razvoja Republike Srbije
* Acknowledgement: The author is thankful for the financial support from the Ministry of Education Science and technological development of the Republic of Serbia (national projects OI 174004). 
Mikromehanički kriterijumi oštećenja i loma biomedicinskih implanata od lergura titana, kobalta i aluminijuma. 
OI 174004  Micromechanical criteria of damage and fracture of biomedical implants of alloys titanium, cobalt and aluminum.
Svojstva prevlake deponovane sa difuziono oksidiranim prahom Mo&O2 primenom APS procesa
ORCID iD: 


http://orcid.org/0000-0003-3983-1605
OBLAST: Hemijske tehnologije

TIP ČLANKA: Izvorni naučni rad

Sažetak:
Prah Mo&O2 ima značajnu ulogu za proizvodnju prevlaka sa povišenom otpornošću na klizanje u uslovima bez primene maziva. Prevlake Mo&O2 imaju mali koeficijent frikcije i dobre karakteristike na habanje pri mehaničkim naprezanjima. U cilju proizvodnje prevlaka visoke tvrdoće, prah Mo&O2 je deponovan plazmom sa optimalnim parametrima. Karakterizacija oblika površine čestica oksidnog praha i površine preloma prevlake izvedena je metodom SEM, a mikrostruktura slojeva primenom svetlosne mikroskopije. Mikrostruktura prevlake se sastoji od lamela Mo i tankih filmova primarnih oksida MoO2 i MoO3 koje okružuju lamele Mo. Analiza dobijenih rezultata pokazala je da slojevi prevlake Mo&O2 sa difuziono oksidiranim česticama Mo imaju strukturu i mehaničke karakteristike, koje omogućuju njenu primenu na površinama radnih delova u uslovima habanja i klizanja trenjem bez maziva.

Ključne reči: Mo&O2, prevlaka, mikrostruktura, mehaničke karakteristike

Properties of the coating deposited with diffusion of oxidized powder Mo&O2 using aps process

ORCID iD: 

http://orcid.org/0000-0003-3983-1605
FIELD: Chemical Technology

ARTICLE TYPE: Original Scientific Paper

ARTICLE LANGUAGE: English 

Summary:

Powder Mo&O2 has an important role for the production of coatings with increased resistance to slide in conditions without the use of lubricants. Mo&O2. Coatings have low coefficient of friction and good abrasion characteristics in mechanical stresses. In aim to produce coatings of high hardness, powder Mo&O2 is plasma deposited with optimal parameters. Characterization of the surface shape of the particles of the oxide powder and the fracture surface coating is performed by SEM, a microstructure layers by using light microscopy. The microstructure of the coating consists of a lamellae Mo i primary oxide thin film MoO3 and MoO2, which surrounding the lamellae Mo. Analysis of the obtained results showed that the coating layers of Mo&O2 with the diffusion oxidized Mo particles have a structure and mechanical characteristics, which enable its application in areas of working parts in terms of wear and sliding friction without lubricant.

Keywords: Mo&O2, coatings, microstructure, mechanical properties

Literature
Chen, D., Jordan, E., & Gell, M., 2007, Effect of solution concentration on splat formation and coating microstructure using the solution precursor plasma spray process, Surface & Coatings Technology, 202, pp.2132-2138.
Jullien, C., Khelfa, A., Hussain, O.M. and Nazri, G.A., 1995, Synthesis and characterization of flash-evaporated MoO3 thin films, Journal of Crystal Growth, 156(3), p.235.

Lyo, I.W. Ahn, H.S. Lim, D.S., 2003, Microstructure and tribological properties of plasmasprayed chromium oxide-molybdenum oxide composite coatings. Surface & Coatings Technology 163, pp.413-421.

Modi, S.C., Calla, E., 2001, A study of high-velocity combustion wire molybdenum coatings, Journal of Thermal spray technology, 2001, 10(3), pp. 480-486.

Mrdak, M., Kakaš, D., Pović, Đ., 2005, Characterisation of APS-Mo wear resistant coatings, pp.235-239, BALKANTRIB '05, 5th International conference on tribology, Srbija, Kragujevac, 15-18.
Mrdak, M., 2016, Properties of the ZrO2MgO/MgZrO3NiCr/NiCr triple-layer thermal barrier coating deposited by the atmospheric plasma spray process, Vojnotehnički glasnik / Military Technical Coуrier, 64(2), pp.411-430.
Mrdak, M.R., 2016, Characterization of Cu10wt.%Al intermetallic coatings applied by the atmospheric plasma spraying process, Vojnotehnički glasnik, 64(4), pp. 949-965.

Salhi, Z., Klein, D., Gougeon, P., Coddet, C., 2005, Development of coating by thermal plasma spraying under very low-pressure condition <1 mbar, Vacuum 77, pp.145–150.
Solak, N., Ustel, F., Urgen, M., Aydin, S., Cakir, A.F., 2003, Oxidation behavior of molybdenum nitride coatings, Surface & Coatings Technology 174, pp.713-719.

Suszko, T., Gulbinski, W., Jagielski, J., 2005, The role of surface oxidation in friction processes on molybdenum nitride thin films, Surface & Coatings Technology 194(2-3), pp.319-324.

Turbojet Engine – Standard Practices Manual PN 582005, 2002, Pratt & Whitney, East Hartford, USA.

Vardelle, M., Vardelle, A. and Leger, A.C., 1994, J. Thermal Spray Technol. 4, pp.50–58.

Vencl, A., Arostegui, S., Favaro, G., Zivic, F., Mrdak, M., Mitrović, S., Popovic, V., 2011, Evaluation of adhesion/cohesion bond strength of the thick plasma spray coatings by scratch testing on coatings cross-sections, Tribology International, 44(11), pp.1281-1288. 

Yongqing, F., Jun, W., Andrew, W., 2000, Some considerations on the mitigation of fretting damage by the application of surface-modification technologies, Journal of Materials Processing Technology, 99, pp.231-245.
