Mihailo R. Mrdak, Research and Development Center 
IMTEL Communications a. d., Belgrade
Ministarstvo obrazovanja i nauke Republike Srbije
* Acknowledgement: The author is thankful for the financial support from the Ministry of Education and Science of the Republic of Serbia (national projects OI 174004, TR 34016).

Razvoj tehnologije izrade obloge i jezgra na bazi domaćih sirovina za proizvodnju specijalnih obloženih elektroda namenjenih za elektrolučno zavarivanje.
TR 34016 Development of technology production cladding and core on based local raw materials for the production of specialty coated electrodes designed for arc welding.
------------------------------

Mikromehanički kriterijumi oštećenja i loma biomedicinskih implanata od lergura titana,kobalta i aluminijuma.
OI 174004  Micromechanical criteria of damage and fracture of biomedical implants of alloys titanium, cobalt and aluminum.
Svojstva troslojne termo barijerne prevlake ZrO2MgO/ MgZrO3NiCr/ NiCr deponovane atmosferskim plazma sprej procesom
OBLAST: hemijske tehnologije

VRSTA ČLANKA: originalni naučni rad

Sažetak:
U radu su prikazani rezultati ispitivanja termo-barijernih slojeva TBC-ZrO2MgO/MgZrO3NiCr/NiCr koji su deponovani plazma sprej procesom na atmosferskom pritisku na substratima od legure Al. U cilju dobijanja strukturnih i mehaničkih osobina slojeva, koji će obezbediti dobru toplotnu i abrazivnu zaštitu zadnjim krilima aviona J-22 kod ispaljivanja raketa munje i groma, izvršena je depozicija tri tipa praha na substratima od legure Al debljine 0,6mm. Ova studija opisuje postupak korišćenja troslojne TBC prevlake kao izbor dobre kombinacije, od mnogo raspoloživih mogućnosti, koja daje dobar kompromis između toplotne zaštite i otpornosti na abraziju za zaštitu zadnjih krila aviona. Studija se uglavnom bazira na eksperimentalnom pristupu. Procena mehaničkih osobina slojeva je urađena ispitivanjem mikrotvrdoće metodom HV0.3 i čvrstoće spoja ispitivanjem na zatezanje. Struktura slojeva je ispitana metodom svetlosne mikroskopije i površina ZrO2MgO keramičkih slojeva metodom skening elektronske mikroskopije (SEM(. Toplotna zaštita TBC slojeva i otpornost na abraziju ispitana je u tunelu Vojnotehničkog instituta Žarkovo. Na osnovu dobijenih karakteristika površinskih slojeva i simuliranja ispaljivanja rakete, troslojni sistem TBC prevlake se pokazao pouzdanim.
Ključne reči: ZrO224%MgO, MgZrO335%NiCr, Ni20%Cr, mikrostruktura, poroznost, plazma prskanje, termo abrazivna barijera.

Properties three layer thermal barrier coating ZrO2MgO/MgZrO3NiCr/NiCr deposited atmospheric plasma spray process
FIELD: Chemical Technology

ARTICLE  TYPE: Original Scientific Paper
This paper presents the results of thermal barrier layers that are deposited TBC-ZrO2MgO/MgZrO3NiCr/NiCr plasma spray process at atmospheric pressure on substrates of Al alloys. In order to obtain the structural and mechanical properties of the layers, which will provide good heat and abrasion protection rear wing aircraft J-22 with firing missiles and lightning strikes, the deposition was carried out three types of powder on substrates of Al alloy 0.6 mm thick. This study describes the use of three-layer TBC coatings as well as a good selection of combinations, of many available possibly, which provides a good compromise between thermal protection and abrasion resistance to protect final wing aircraft. The study is mainly based on the experimental approach. Evaluation of mechanical properties of the layers is made of micro hardness testing method HV0.3 and bond strength tensile testing. The layer structure was examined using light microscopy and surface ZrO2MgO ceramic layers using scanning electron microscopy SEM. hermal protection TBC layers and abrasion resistance was tested in the tunnel Technical Institute Zarkovo. On the basis of the characteristics of the surface layers and simulating the firing of rockets, three-layer TBC coating system is reliable.

Keywords: ZrO224% MgO, MgZrO335% NiCr, NI20% Cr, microstructure, porosity, plasma spray, thermal barrier abrasive.

LITERATURE 

Boutz, M.M.R., Winnubst, A.J.A., Burggraaf, A.J., 1994, Yttria-ceria stabilized tetragonal zirconia polycrystals: Sintering, grain growth and grain boundary segregation, Journal of the European Ceramic Society, 13(2), pp.89-102.

Brossard, S., Munroe, P.R., Tran, A.T.T., Hyland, M.M., 2010, Study of the microstructure of NiCr splats plasma sprayed on to stainless steel substrates by TEM, Surface and Coatings Technology, 204(9-10), pp.1608-1615.

Celik E, Avci E, Yilmaz F., 1997, Evaluation of Interface Reactions in Thermal Barrier Ceramic Coatings, Surf. Coatings Technol., 97, pp.361–365.
Chevalier, J., Gremillard, L., Virkar, A.V., Clarke, D.R., 2009, The tetragonal-monoclinic transformation in zirconia: Lessons learned and future trends, Journal of the American Ceramic Society, 92(9), pp.1901-1920.

Demirkiran, A.S., Avci, E., 1999, Evaluation of functionally gradient coatings produced by plasma-spray technique.Surf. Coat. Technol. 116–119, pp.292–295.

Garvie ,R.C., 1970, Zirconium dioxide and some of its binary systems, in: Alper, A.M., (ed.), High-temperature oxides, Vol. 5–II, Academic Press, New York, pp.117–166.

Garvie, R.C., Hannink, R.H.J., and Pascoe, R.T., 1975, ‘Ceramic steel?’, Nature, 258, pp.703-704.

Guo, H., Yao, R. and Zhpu, L., 2011, in ‘Thermal barrier coatings’, (ed. Xu, H.and Guo, H.) Cambridge, Woodhead Publishing Limited, pp.161–174.

Johner,G., Schweitzer, K.K., 1984, Thermal barrier coatings for jet engine improvement, Thin Solid Films, 119(3), pp.301-315.

Li, C.-J. and Ohmori, A., 2002, Relationships Between the Microstructure and Properties of Thermally Sprayed Deposits, J. Thermal Spray Technol., 11(3), pp.365-374.
Material Product Data Sheet, 2012, Metco 43F-NS Nickel - 20% Chromium  Powders. Sulzer Metco. DSMTS–0109.0. 

Material Product Data Sheet, 2012, Metco 303NS-1 Magnesium Zirconate – Nickel Chromium Cermet Blends. Sulzer Metco. DSMTS–0070.0. 

Metco 210NS-1 Magnesium Zirconate Powder, 2000, Sulzer Metco.Technical bulletin 10-289.

Miyamoto, Y., Kaysser, W.A., Rabin, B.H., Kawasaki, A., Ford, R.G., 1999, Functionally Graded Materials: Design, Processing and Applications,Kluwer Academic Publisher, Boston, p.100.

Mrdak, M., 2013, Ispitivanje mehaničkih i strukturnih osobina prevlaka otpornih na eroziju i visoke temperature, pp.426-432, SERBIATRIB '13, 13th International Conference on Tribology, Serbia, Kragujevac, 15-17.

Mrdak, M., Vencl, A., Nedeljkovic, B., Stanković, M., 2013, Influence of plasma spraying parameters on properties of the thermal barrier coatings, Materials Science and Technology, 29(5), pp.559-567.
Mrdak, M., Rakin, M., Medjo, B., Bajić, N., 2015, Experimental Study of Insulating Properties and Behaviour of Thermal Barrier Coating Systems in Thermo Cyclic Conditions, Materials & Design, 67, pp.337-343. 

Mrdak, M., 2015, Investigation of the influence of plasma spray sealing coatings on the effect of sealing the TV2- 117A turbojet engine compressor, Vojnotehnički glasnik/MilitaryTechnical Courier, 63(1), pp.32-55. 
Nicoll, A.R., 1984, The environment – high temperature oxidation and hot corrosion, u: CEI Course on High Temperature Materials and Coatings, Finland.

Turbojet Engine – Standard Practices Manual (PN 582005), 2002, Pratt & Whitney, East Hartford, USA.
